CHAPTER 6

MECHANICAL PROPERTIES OF METALS

PROBLEM SOLUTIONS


Concepts of Stress and Strain


6.1  Using mechanics of materials principles (i.e., equations of mechanical equilibrium applied to a free-body diagram), derive Equations 6.4a and 6.4b.


Solution

This problem asks that we derive Equations 6.4a and 6.4b, using mechanics of materials principles.  In Figure (a) below is shown a block element of material of cross-sectional area A that is subjected to a tensile force P.  Also represented is a plane that is oriented at an angle  referenced to the plane perpendicular to the tensile axis;  the area of this plane is A' = A/cos .  In addition, and the forces normal and parallel to this plane are labeled as P' and V', respectively.  Furthermore, on the left-hand side of this block element are shown force components that are tangential and perpendicular to the inclined plane.  In Figure (b) are shown the orientations of the applied stress , the normal stress to this plane ', as well as the shear stress ' taken parallel to this inclined plane.  In addition, two coordinate axis systems in represented in Figure (c):  the primed x and y axes are referenced to the inclined plane, whereas the unprimed x axis is taken parallel to the applied stress.

[image: image1.png]P 7/:

Nt
P sin 6 P cos/e/ —————

e

C <— T

e

b (©)
@) (b)





Normal and shear stresses are defined by Equations 6.1 and 6.3, respectively.  However, we now chose to express these stresses in terms (i.e., general terms) of normal and shear forces (P and V) as


[image: image2.wmf]

[image: image3.wmf]
For static equilibrium in the x' direction the following condition must be met:


[image: image4.wmf]
which means that


[image: image5.wmf]
Or that


[image: image6.wmf]
Now it is possible to write an expression for the stress 
[image: image7.wmf] in terms of P' and A' using the above expression and the relationship between A and A' [Figure (a)]:


[image: image8.wmf]

[image: image9.wmf]
However, it is the case that P/A = ;  and, after making this substitution into the above expression, we have Equation 6.4a--that is


[image: image10.wmf]

Now, for static equilibrium in the y' direction, it is necessary that


[image: image11.wmf]

[image: image12.wmf]
Or


[image: image13.wmf]
We now write an expression for ' as


[image: image14.wmf]
And, substitution of the above equation for V' and also the expression for A' gives


[image: image15.wmf]

[image: image16.wmf]

[image: image17.wmf]

[image: image18.wmf]
which is just Equation 6.4b.


6.2  (a) Equations 6.4a and 6.4b are expressions for normal (σ′) and shear (τ′) stresses, respectively, as a function of the applied tensile stress (σ) and the inclination angle of the plane on which these stresses are taken (θ of Figure 6.4). Make a plot on which is presented the orientation parameters of these expressions (i.e., cos2 θ and sin θ cos θ) versus θ.


(b) From this plot, at what angle of inclination is the normal stress a maximum?


(c) Also, at what inclination angle is the shear stress a maximum?


Solution

(a)  Below are plotted curves of cos2 (for 
[image: image19.wmf]) and sin cos  (for ') versus .

[image: image20.png]c0s20, sin@ cos@

1.0

0.8

0.6

0.4

0.2

0.0
0

sin @ cos@O

10

20

30

40 50

0 (degrees)

60

70

80

90





(b)  The maximum normal stress occurs at an inclination angle of 0.


(c)  The maximum shear stress occurs at an inclination angle of 45.


Stress-Strain Behavior

6.3  A specimen of aluminum having a rectangular cross section 10 mm ( 12.7 mm (0.4 in. ( 0.5 in.) is pulled in tension with 35,500 N (8000 lbf) force, producing only elastic deformation.  Calculate the resulting strain.


Solution

This problem calls for us to calculate the elastic strain that results for an aluminum specimen stressed in tension.  The cross-sectional area is just (10 mm) ( (12.7 mm) = 127 mm2 (= 1.27 ( 10-4 m2 = 0.20 in.2);  also, the elastic modulus for Al is given in Table 6.1 as 69 GPa (or 69 ( 109 N/m2).  Combining Equations 6.1 and 6.5 and solving for the strain yields


[image: image21.wmf]

6.4  A cylindrical specimen of a titanium alloy having an elastic modulus of 107 GPa (15.5 ( 106 psi) and an original diameter of 3.8 mm (0.15 in.) will experience only elastic deformation when a tensile load of 2000 N (450 lbf) is applied.  Compute the maximum length of the specimen before deformation if the maximum allowable elongation is 0.42 mm (0.0165 in.).


Solution

We are asked to compute the maximum length of a cylindrical titanium alloy specimen (before deformation) that is deformed elastically in tension.  For a cylindrical specimen


[image: image22.wmf]
where d0 is the original diameter.  Combining Equations 6.1, 6.2, and 6.5 and solving for l0 leads to


[image: image23.wmf]

[image: image24.wmf]
= 0.255 m = 255 mm (10.0 in.)


6.5  A steel bar 100 mm (4.0 in.) long and having a square cross section 20 mm (0.8 in.) on an edge is pulled in tension with a load of 89,000 N (20,000 lbf), and experiences an elongation of 0.10 mm (4.0 ( 10-3 in.).  Assuming that the deformation is entirely elastic, calculate the elastic modulus of the steel.


Solution

This problem asks us to compute the elastic modulus of steel.  For a square cross-section, A0 = 
[image: image25.wmf], where b0 is the edge length.  Combining Equations 6.1, 6.2, and 6.5 and solving for E, leads to


[image: image26.wmf]

[image: image27.wmf]
= 223 ( 109 N/m2 = 223 GPa  (31.3 ( 106 psi)


6.6  Consider a cylindrical titanium wire 3.0 mm (0.12 in.) in diameter and 2.5 ( 104 mm (1000 in.) long.  Calculate its elongation when a load of 500 N (112 lbf) is applied.  Assume that the deformation is totally elastic.


Solution

In order to compute the elongation of the Ti wire when the 500 N load is applied we must employ Equations 6.1, 6.2, and 6.5.  Solving for ∆l and realizing that for Ti, E = 107 GPa (15.5 ( 106 psi) (Table 6.1),


[image: image28.wmf]

[image: image29.wmf]

6.7  For a bronze alloy, the stress at which plastic deformation begins is 275 MPa (40,000 psi), and the modulus of elasticity is 115 GPa (16.7 ( 106 psi).


(a) What is the maximum load that may be applied to a specimen with a cross-sectional area of 325 mm2 (0.5 in.2) without plastic deformation?


(b) If the original specimen length is 115 mm (4.5 in.), what is the maximum length to which it may be stretched without causing plastic deformation?


Solution

(a)  This portion of the problem calls for a determination of the maximum load that can be applied without plastic deformation (Fy).  Taking the yield strength to be 275 MPa, and employment of Equation 6.1 leads to


[image: image30.wmf]
= 89,375 N   (20,000 lbf)


(b)  The maximum length to which the sample may be deformed without plastic deformation is determined from Equations 6.2 and 6.5 as


[image: image31.wmf]

[image: image32.wmf]

6.8  A cylindrical rod of copper (E = 110 GPa, 16 ( 106 psi) having a yield strength of 240 MPa (35,000 psi) is to be subjected to a load of 6660 N (1500 lbf).  If the length of the rod is 380 mm (15.0 in.), what must be the diameter to allow an elongation of 0.50 mm (0.020 in.)?


Solution

This problem asks us to compute the diameter of a cylindrical specimen of copper in order to allow an elongation of 0.50 mm.  Employing Equations 6.1, 6.2, and 6.5, assuming that deformation is entirely elastic


[image: image33.wmf]
Or, solving for d0

[image: image34.wmf]

[image: image35.wmf]
= 7.65 ( 10-3 m = 7.65 mm  (0.30 in.)


6.9  Compute the elastic moduli for the following metal alloys, whose stress-strain behaviors may be observed in the “Tensile Tests” module of Virtual Materials Science and Engineering (VMSE):  (a)  titanium, (b) tempered steel, (c) aluminum, and (d) carbon steel.  How do these values compare with those presented in Table 6.1 for the same metals?


Solution

The elastic modulus is the slope in the linear elastic region (Equation 6.10) as


[image: image36.wmf]
Since stress-strain curves for all of the metals/alloys pass through the origin, we make take 1 = 0 and 1 = 0.  Determinations of 2 and 2 are possible by moving the cursor to some arbitrary point in the linear region of the curve and then reading corresponding values in the “Stress” and “Strain” windows that are located below the plot.

(a)  For the titanium alloy, we selected 2 = 404.2 MPa with its corresponding 2 = 0.0038.  Therefore,


[image: image37.wmf]

The elastic modulus for titanium given in Table 6.1 is 107 GPa, which is in very good agreement with this value.


(b)  For the tempered steel, we selected 2 = 962.2 MPa with its corresponding 2 = 0.0047.  Therefore,


[image: image38.wmf]

The elastic modulus for steel given in Table 6.1 is 207 GPa, which is in reasonably good agreement with this value.


(c)  For the aluminum, we selected 2 = 145.1 MPa with its corresponding 2 = 0.0021.  Therefore,


[image: image39.wmf]

The elastic modulus for aluminum given in Table 6.1 is 69 GPa, which is in excellent agreement with this value.


(d)  For the carbon steel, we selected 2 = 129 MPa with its corresponding 2 = 0.0006.  Therefore,


[image: image40.wmf]

The elastic modulus for steel given in Table 6.1 is 207 GPa, which is in reasonable agreement with this value.


6.10  Consider a cylindrical specimen of a steel alloy (Figure 6.21) 10.0 mm (0.39 in.) in diameter and 75 mm (3.0 in.) long that is pulled in tension.  Determine its elongation when a load of 20,000 N (4,500 lbf) is applied.


Solution

This problem asks that we calculate the elongation ∆l of a specimen of steel the stress-strain behavior of which is shown in Figure 6.21.  First it becomes necessary to compute the stress when a load of 20,000 N is applied using Equation 6.1 as


[image: image41.wmf]
Referring to Figure 6.21, at this stress level we are in the elastic region on the stress-strain curve, which corresponds to a strain of 0.0012.  Now, utilization of Equation 6.2 to compute the value of l

[image: image42.wmf]

6.11  Figure 6.22 shows, for a gray cast iron, the tensile engineering stress–strain curve in the elastic region. Determine (a) the tangent modulus at 10.3 MPa (1500 psi), and (b) the secant modulus taken to 6.9 MPa (1000 psi).


Solution

(a)  This portion of the problem asks that the tangent modulus be determined for the gray cast iron, the stress-strain behavior of which is shown in Figure 6.22.  In the figure below is shown a tangent draw on the curve at a stress of 10.3 MPa (1500 psi).

[image: image43.png]Stress (MPa)

2500

[ T T l T
— 2000
— 1500
— 1000
— 500
| by ey sd 0],
0.002 0.004 0.006 0.008 0.010

Strain

Stress (psi)




The slope of this line (i.e., ∆/∆), the tangent modulus, is computed as follows:


[image: image44.wmf]

(b)  The secant modulus taken from the origin is calculated by taking the slope of a secant drawn from the origin through the stress-strain curve at 6.9 MPa (1,000 psi).  This secant is drawn on the curve shown below:

[image: image45.png]Stress (MPa)

T Y M|

0.002

0.004 0.006 0.008
Strain

2500

2000

1000

500

0
0.010

Stress (psi)




The slope of this line (i.e., ∆/∆), the secant modulus, is computed as follows:


[image: image46.wmf]

6.12 As noted in Section 3.15, for single crystals of some substances, the physical properties are anisotropic; that is, they are dependent on crystallographic direction. One such property is the modulus of elasticity. For cubic single crystals, the modulus of elasticity in a general [uvw] direction, Euvw, is described by the relationship

[image: image47.wmf]
where 
[image: image48.wmf] and 
[image: image49.wmf] are the moduli of elasticity in [100] and [111] directions, respectively; α, β, and γ are the cosines of the angles between [uvw] and the respective [100], [010], and [001] directions. Verify that the 
[image: image50.wmf] values for aluminum, copper, and iron in Table 3.3 are correct.



Solution

We are asked, using the equation given in the problem statement, to verify that the modulus of elasticity values along [110] directions given in Table 3.3 for aluminum, copper, and iron are correct.  The , , and  parameters in the equation correspond, respectively, to the cosines of the angles between the [110] direction and [100], [010] and [001] directions.  Since these angles are 45, 45, and 90, the values of , , and  are 0.707, 0.707, and 0, respectively.  Thus, the given equation takes the form


[image: image51.wmf]

[image: image52.wmf]

[image: image53.wmf]
Utilizing the values of E<100> and E<111> from Table 3.3 for Al


[image: image54.wmf]
Which leads to, E<110> = 72.6 GPa, the value cited in the table.


For Cu,


[image: image55.wmf]
Thus, E<110> = 130.3 GPa, which is also the value cited in the table.


Similarly, for Fe


[image: image56.wmf]
And E<110> = 210.5 GPa, which is also the value given in the table.


6.13  In Section 2.6 it was noted that the net bonding energy EN between two isolated positive and negative ions is a function of interionic distance r as follows:



[image: image57.wmf]
(6.25)

where A, B, and n are constants for the particular ion pair. Equation 6.25 is also valid for the bonding energy between adjacent ions in solid materials. The modulus of elasticity E is proportional to the slope of the interionic force–separation curve at the equilibrium interionic separation; that is,


[image: image58.wmf]
Derive an expression for the dependence of the modulus of elasticity on these A, B, and n parameters (for the two-ion system) using the following procedure:


1. Establish a relationship for the force F as a function of r, realizing that


[image: image59.wmf]

2. Now take the derivative dF/dr.


3. Develop an expression for r0, the equilibrium separation. Since r0 corresponds to the value of r at the minimum of the EN-versus-r curve (Figure 2.8b), take the derivative dEN/dr, set it equal to zero, and solve for r, which corresponds to r0.


4. Finally, substitute this expression for r0 into the relationship obtained by taking dF/dr.



Solution

This problem asks that we derive an expression for the dependence of the modulus of elasticity, E, on the parameters A, B, and n in Equation 6.25.  It is first necessary to take dEN/dr in order to obtain an expression for the force F;  this is accomplished as follows:


[image: image60.wmf]

[image: image61.wmf]
The second step is to set this dEN/dr expression equal to zero and then solve for r (= r0).  The algebra for this procedure is carried out in Problem 2.14, with the result that


[image: image62.wmf]
Next it becomes necessary to take the derivative of the force (dF/dr), which is accomplished as follows:


[image: image63.wmf]

[image: image64.wmf]
Now, substitution of the above expression for r0 into this equation yields


[image: image65.wmf]
which is the expression to which the modulus of elasticity is proportional.


6.14  Using the solution to Problem 6.13, rank the magnitudes of the moduli of elasticity for the following hypothetical X, Y, and Z materials from the greatest to the least. The appropriate A, B, and n parameters (Equation 6.25) for these three materials are tabulated below; they yield EN in units of electron volts and r in nanometers:
	Material
	A
	B
	n

	X
	2.5
	2.0 × 10–5
	8

	Y
	2.3
	8.0 × 10–6
	10.5

	Z
	3.0
	1.5 × 10–5
	9




Solution

This problem asks that we rank the magnitudes of the moduli of elasticity of the three hypothetical metals X, Y, and Z.  From Problem 6.13, it was shown for materials in which the bonding energy is dependent on the interatomic distance r according to Equation 6.25, that the modulus of elasticity E is proportional to


[image: image66.wmf]

For metal X, A = 2.5, B = 2.0 ( 10-5, and n = 8.  Therefore,


[image: image67.wmf]
= 1097


For metal Y, A = 2.3, B = 8 ( 10-6, and n = 10.5.  Hence


[image: image68.wmf]
= 551


And, for metal Z, A = 3.0, B = 1.5 ( 10-5, and n = 9.  Thus


[image: image69.wmf]
= 1024


Therefore, metal X has the highest modulus of elasticity.


Elastic Properties of Materials

6.15  A cylindrical specimen of aluminum having a diameter of 19 mm (0.75 in.) and length of 200 mm (8.0 in.) is deformed elastically in tension with a force of 48,800 N (11,000 lbf).  Using the data contained in Table 6.1, determine the following:


(a) The amount by which this specimen will elongate in the direction of the applied stress.


(b) The change in diameter of the specimen. Will the diameter increase or decrease?


Solution
 
(a)  We are asked, in this portion of the problem, to determine the elongation of a cylindrical specimen of aluminum.  Combining Equations 6.1, 6.2, and 6.5, leads to


[image: image70.wmf]

[image: image71.wmf]
Or, solving for l (and realizing that E = 69 GPa, Table 6.1), yields

[image: image72.wmf]

[image: image73.wmf]

(b)  We are now called upon to determine the change in diameter, d.  Using Equation 6.8


[image: image74.wmf]
From Table 6.1, for aluminum,  = 0.33.  Now, solving the above expression for ∆d yields


[image: image75.wmf]
= –1.6 ( 10-2 mm  (–6.2 ( 10-4 in.)

The diameter will decrease.


6.16  A cylindrical bar of steel 10 mm (0.4 in.) in diameter is to be deformed elastically by application of a force along the bar axis.  Using the data in Table 6.1, determine the force that will produce an elastic reduction of 3 ( 10-3 mm (1.2 ( 10-4 in.) in the diameter.


Solution

This problem asks that we calculate the force necessary to produce a reduction in diameter of 3 ( 10-3 mm for a cylindrical bar of steel.  For a cylindrical specimen, the cross-sectional area is equal to


[image: image76.wmf]
Now, combining Equations 6.1 and 6.5 leads to 


[image: image77.wmf]
And, since from Equation 6.8


[image: image78.wmf]
Substitution of this equation into the above expression gives


[image: image79.wmf]
And, solving for F leads to


[image: image80.wmf]
From Table 6.1, for steel,  = 0.30 and E = 207 GPa.  Thus,


[image: image81.wmf]
= 16,250 N  (3770 lbf)


6.17  A cylindrical specimen of some alloy 8 mm (0.31 in.) in diameter is stressed elastically in tension.  A force of 15,700 N (3530 lbf) produces a reduction in specimen diameter of 5 ( 10-3 mm (2 ( 10-4 in.).  Compute Poisson's ratio for this material if its modulus of elasticity is 140 GPa (20.3 ( 106 psi).


Solution

This problem asks that we compute Poisson's ratio for the metal alloy.  From Equations 6.5 and 6.1


[image: image82.wmf]
Since the transverse strain x is just


[image: image83.wmf]
and Poisson's ratio is defined by Equation 6.8, then


[image: image84.wmf]

[image: image85.wmf]

6.18  A cylindrical specimen of a hypothetical metal alloy is stressed in compression.  If its original and final diameters are 20.000 and 20.025 mm, respectively, and its final length is 74.96 mm, compute its original length if the deformation is totally elastic.  The elastic and shear moduli for this alloy are 105 GPa and 39.7 GPa, respectively.


Solution

This problem asks that we compute the original length of a cylindrical specimen that is stressed in compression.  It is first convenient to compute the lateral strain x as


[image: image86.wmf]
In order to determine the longitudinal strain z we need Poisson's ratio, which may be computed using Equation 6.9;  solving for  yields


[image: image87.wmf]
Now z may be computed from Equation 6.8 as


[image: image88.wmf]
Now solving for l0 using Equation 6.2


[image: image89.wmf]

[image: image90.wmf]

6.19  Consider a cylindrical specimen of some hypothetical metal alloy that has a diameter of 8.0 mm (0.31 in.).  A tensile force of 1000 N (225 lbf) produces an elastic reduction in diameter of 2.8 ( 10-4 mm (1.10 ( 10-5 in.).  Compute the modulus of elasticity for this alloy, given that Poisson's ratio is 0.30.


Solution

This problem asks that we calculate the modulus of elasticity of a metal that is stressed in tension.  Combining Equations 6.5 and 6.1 leads to


[image: image91.wmf]
From the definition of Poisson's ratio, (Equation 6.8) and realizing that for the transverse strain, x= 
[image: image92.wmf]

[image: image93.wmf]
Therefore, substitution of this expression for z into the above equation yields


[image: image94.wmf]

[image: image95.wmf]

6.20  A brass alloy is known to have a yield strength of 275 MPa (40,000 psi), a tensile strength of 380 MPa (55,000 psi), and an elastic modulus of 103 GPa (15.0 ( 106 psi).  A cylindrical specimen of this alloy 12.7 mm (0.50 in.) in diameter and 250 mm (10.0 in.) long is stressed in tension and found to elongate 7.6 mm (0.30 in.).  On the basis of the information given, is it possible to compute the magnitude of the load that is necessary to produce this change in length?  If so, calculate the load.  If not, explain why.


Solution

We are asked to ascertain whether or not it is possible to compute, for brass, the magnitude of the load necessary to produce an elongation of 7.6 mm (0.30 in.).  It is first necessary to compute the strain at yielding from the yield strength and the elastic modulus, and then the strain experienced by the test specimen.  Then, if

(test) < (yield)

deformation is elastic, and the load may be computed using Equations 6.1 and 6.5.  However, if

(test) > (yield)

computation of the load is not possible inasmuch as deformation is plastic and we have neither a stress-strain plot nor a mathematical expression relating plastic stress and strain.  We compute these two strain values as


[image: image96.wmf]
and


[image: image97.wmf]
Therefore, computation of the load is not possible since (test) > (yield).


6.21 A cylindrical metal specimen 12.7 mm (0.5 in.) in diameter and 250 mm (10 in.) long is to be subjected to a tensile stress of 28 MPa (4000 psi);  at this stress level the resulting deformation will be totally elastic.


(a) If the elongation must be less than 0.080 mm (3.2 ( 10-3 in.), which of the metals in Table 6.1 are suitable candidates?  Why?


(b) If, in addition, the maximum permissible diameter decrease is 1.2 (  10-3 mm (4.7 ( 10-5 in.) when the tensile stress of 28 MPa is applied, which of the metals that satisfy the criterion in part (a) are suitable candidates? Why?



Solution

(a)  This part of the problem asks that we ascertain which of the metals in Table 6.1 experience an elongation of less than 0.080 mm when subjected to a tensile stress of 28 MPa.  The maximum strain that may be sustained, (using Equation 6.2) is just


[image: image98.wmf]
Since the stress level is given (50 MPa), using Equation 6.5 it is possible to compute the minimum modulus of elasticity which is required to yield this minimum strain.  Hence


[image: image99.wmf]
Which means that those metals with moduli of elasticity greater than this value are acceptable candidates—namely, brass, Cu, Ni, steel, Ti and W.


(b)  This portion of the problem further stipulates that the maximum permissible diameter decrease is 1.2 ( 10-3 mm when the tensile stress of 28 MPa is applied.  This translates into a maximum lateral strain x(max) as


[image: image100.wmf]
But, since the specimen contracts in this lateral direction, and we are concerned that this strain be less than 9.45 ( 10-5, then the criterion for this part of the problem may be stipulated as 
[image: image101.wmf]
Now, Poisson’s ratio is defined by Equation 6.8 as


[image: image102.wmf]
For each of the metal alloys let us consider a possible lateral strain, 
[image: image103.wmf]. Furthermore, since the deformation is elastic, then, from Equation 6.5, the longitudinal strain, z is equal to


[image: image104.wmf]
Substituting these expressions for x and z into the definition of Poisson’s ratio we have


[image: image105.wmf]
which leads to the following:


[image: image106.wmf]
Using values for  and E found in Table 6.1 for the six metal alloys that satisfy the criterion for part (a), and for  = 28 MPa, we are able to compute a 
[image: image107.wmf] for each alloy as follows:


[image: image108.wmf]

[image: image109.wmf]

[image: image110.wmf]

[image: image111.wmf]

[image: image112.wmf]

[image: image113.wmf]
Thus, of the above six alloys, only brass will have a negative transverse strain that is greater than 9.45 ( 10-5.  This means that the following alloys satisfy the criteria for both parts (a) and (b) of the problem:  copper, titanium, nickel, steel, and tungsten.


6.22  Consider the brass alloy for which the stress-strain behavior is shown in Figure 6.12.  A cylindrical specimen of this material 6 mm (0.24 in.) in diameter and 50 mm (2 in.) long is pulled in tension with a force of 5000 N (1125 lbf).  If it is known that this alloy has a Poisson's ratio of 0.30, compute:  (a) the specimen elongation, and (b) the reduction in specimen diameter.


Solution

(a)  This portion of the problem asks that we compute the elongation of the brass specimen.  The first calculation necessary is that of the applied stress using Equation 6.1, as


[image: image114.wmf]
From the stress-strain plot in Figure 6.12, this stress corresponds to a strain of about 2.0 ( 10-3.  From the definition of strain, Equation 6.2


[image: image115.wmf]

(b)  In order to determine the reduction in diameter ∆d, it is necessary to use Equation 6.8 and the definition of lateral strain (i.e., x = ∆d/d0) as follows


[image: image116.wmf]
= –3.6 ( 10-3 mm  (–1.4 ( 10-4 in.)


6.23 A cylindrical rod 100 mm long and having a diameter of 10.0 mm is to be deformed using a tensile load of 27,500 N.  It must not experience either plastic deformation or a diameter reduction of more than 7.5 ( 10-3 mm. Of the materials listed as follows, which are possible candidates?  Justify your choice(s).

	Material
	Modulus of Elasticity

(GPa)
	Yield Strength

(MPa)
	Poisson’s Ratio

	Aluminum alloy
	70
	200
	0.33

	Brass alloy
	101
	300
	0.34

	Steel alloy
	207
	400
	0.30

	Titanium alloy
	107
	650
	0.34




Solution

This problem asks that we assess the four alloys relative to the two criteria presented.  The first criterion is that the material not experience plastic deformation when the tensile load of 27,500 N is applied;  this means that the stress corresponding to this load not exceed the yield strength of the material.  Upon computing the stress


[image: image117.wmf]
Of the alloys listed, the Ti and steel alloys have yield strengths greater than 350 MPa.


Relative to the second criterion (i.e., that d be less than 7.5 ( 10-3 mm), it is necessary to calculate the change in diameter ∆d for these three alloys.  From Equation 6.8


[image: image118.wmf]
Now, solving for ∆d from this expression,


[image: image119.wmf]

For the steel alloy


[image: image120.wmf]
Therefore, the steel is a candidate.


For the Ti alloy


[image: image121.wmf]
Hence, the titanium alloy is not a candidate.


6.24  A cylindrical rod 380 mm (15.0 in.) long, having a diameter of 10.0 mm (0.40 in.), is to be subjected to a tensile load. If the rod is to experience neither plastic deformation nor an elongation of more than 0.9 mm (0.035 in.) when the applied load is 24,500 N (5500 lbf), which of the four metals or alloys listed below are possible candidates? Justify your choice(s).

	Material
	Modulus of Elasticity

(GPa)
	Yield Strength

(MPa)
	Tensile Strength

(MPa)

	Aluminum alloy
	70
	255
	420

	Brass alloy
	100
	345
	420

	Copper
	110
	250
	290

	Steel alloy
	207
	450
	550




Solution

This problem asks that we ascertain which of four metal alloys will not (1) experience plastic deformation, and (2) elongate more than 0.9 mm when a tensile load of 24,500 N is applied.  It is first necessary to compute the stress using Equation 6.1;  a material to be used for this application must necessarily have a yield strength greater than this value.  Thus,


[image: image122.wmf]
Of the metal alloys listed, only brass and steel have yield strengths greater than this stress.


Next, we must compute the elongation produced in both brass and steel using Equations 6.2 and 6.5 in order to determine whether or not this elongation is less than 0.9 mm.  For brass


[image: image123.wmf]
Thus, brass is not a candidate.  However, for steel


[image: image124.wmf]
Therefore, of these four alloys, only steel satisfies the stipulated criteria.


Tensile Properties

6.25  Figure 6.21 shows the tensile engineering stress–strain behavior for a steel alloy.


(a) What is the modulus of elasticity?


(b) What is the proportional limit?


(c) What is the yield strength at a strain offset of 0.002?


(d) What is the tensile strength?


Solution

Using the stress-strain plot for a steel alloy (Figure 6.21), we are asked to determine several of its mechanical characteristics.


(a)  The elastic modulus is just the slope of the initial linear portion of the curve;  or, from the inset and using Equation 6.10


[image: image125.wmf]
The value given in Table 6.1 is 207 GPa.


(b)  The proportional limit is the stress level at which linearity of the stress-strain curve ends, which is approximately 300 MPa (43,500 psi).


(c)  The 0.002 strain offset line intersects the stress-strain curve at approximately 400 MPa (58,000 psi).


(d)  The tensile strength (the maximum on the curve) is approximately 515 MPa (74,700 psi).


6.26  A cylindrical specimen of a brass alloy having a length of 60 mm (2.36 in.) must elongate only 10.8 mm (0.425 in.) when a tensile load of 50,000 N (11,240 lbf) is applied.  Under these circumstances, what must be the radius of the specimen?  Consider this brass alloy to have the stress-strain behavior shown in Figure 6.12.


Solution

We are asked to calculate the radius of a cylindrical brass specimen in order to produce an elongation of 10.8 mm when a load of 50,000 N is applied.  It first becomes necessary to compute the strain corresponding to this elongation using Equation 6.2 as


[image: image126.wmf]
From Figure 6.12, a stress of 420 MPa (61,000 psi) corresponds to this strain.  Since for a cylindrical specimen, stress, force, and initial radius r0 are related as


[image: image127.wmf]
then


[image: image128.wmf]

6.27 A load of 85,000 N (19,100 lbf) is applied to a cylindrical specimen of a steel alloy (displaying the stress–strain behavior shown in Figure 6.21) that has a cross-sectional diameter of 15 mm (0.59 in.).


(a) Will the specimen experience elastic and/or plastic deformation? Why?


(b) If the original specimen length is 250 mm (10 in.), how much will it increase in length when this load is applied?


Solution

This problem asks us to determine the deformation characteristics of a steel specimen, the stress-strain behavior for which is shown in Figure 6.21.


(a)  In order to ascertain whether the deformation is elastic or plastic, we must first compute the stress, then locate it on the stress-strain curve, and, finally, note whether this point is on the elastic or plastic region.  Thus, from Equation 6.1


[image: image129.wmf]
The 481 MPa point is beyond the linear portion of the curve, and, therefore, the deformation will be both elastic and plastic.


(b)  This portion of the problem asks us to compute the increase in specimen length.  From the stress-strain curve, the strain at 481 MPa is approximately 0.0135.  Thus, from Equation 6.2


[image: image130.wmf]

6.28  A bar of a steel alloy that exhibits the stress-strain behavior shown in Figure 6.21 is subjected to a tensile load; the specimen is 300 mm (12 in.) long, and of square cross section 4.5 mm (0.175 in.) on a side.

(a)  Compute the magnitude of the load necessary to produce an elongation of 0.45 mm (0.018 in.).


(b)  What will be the deformation after the load has been released?


Solution

(a)  We are asked to compute the magnitude of the load necessary to produce an elongation of 0.45 mm for the steel displaying the stress-strain behavior shown in Figure 6.21.  First, calculate the strain, and then the corresponding stress from the plot.


[image: image131.wmf]
This is near the end of the elastic region;  from the inset of Figure 6.21, this corresponds to a stress of about 300 MPa (43,500 psi).  Now, from Equation 6.1


[image: image132.wmf]
in which b is the cross-section side length.  Thus,


[image: image133.wmf]

(b)  After the load is released there will be no deformation since the material was strained only elastically.


6.29  A cylindrical specimen of aluminum having a diameter of 0.505 in. (12.8 mm) and a gauge length of 2.000 in. (50.800 mm) is pulled in tension.  Use the load–elongation characteristics tabulated below to complete parts (a) through (f).
	Load
	Length

	N
	lbf
	mm
	in.

	0
	0
	50.800
	2.000

	7,330
	1,650
	50.851
	2.002

	15,100
	3,400
	50.902
	2.004

	23,100
	5,200
	50.952
	2.006

	30,400
	6,850
	51.003
	2.008

	34,400
	7,750
	51.054
	2.010

	38,400
	8,650
	51.308
	2.020

	41,300
	9,300
	51.816
	2.040

	44,800
	10,100
	52.832
	2.080

	46,200
	10,400
	53.848
	2.120

	47,300
	10,650
	54.864
	2.160

	47,500
	10,700
	55.880
	2.200

	46,100
	10,400
	56.896
	2.240

	44,800
	10,100
	57.658
	2.270

	42,600
	9,600
	58.420
	2.300

	36,400
	8,200
	59.182
	2.330

	Fracture



(a) Plot the data as engineering stress versus engineering strain.


(b) Compute the modulus of elasticity.


(c) Determine the yield strength at a strain offset of 0.002.


(d) Determine the tensile strength of this alloy.


(e) What is the approximate ductility, in percent elongation?


(f) Compute the modulus of resilience.



Solution

This problem calls for us to make a stress-strain plot for aluminum, given its tensile load-length data, and then to determine some of its mechanical characteristics.


(a)  The data are plotted below on two plots:  the first corresponds to the entire stress-strain curve, while for the second, the curve extends to just beyond the elastic region of deformation.

[image: image134.png]0.10

400

1
o
o
Al

300 I

(BdN) SSa11S

100

0.00

Strain




[image: image135.png]Stress (MPa)

300

200

100

0
0.000

0.002

0.004

0.006

Strain

0.008

0.010

0.012





(b)  The elastic modulus is the slope in the linear elastic region (Equation 6.10) as


[image: image136.wmf]

(c)  For the yield strength, the 0.002 strain offset line is drawn dashed.  It intersects the stress-strain curve at approximately 285 MPa (41,000 psi ).


(d)  The tensile strength is approximately 370 MPa (54,000 psi), corresponding to the maximum stress on the complete stress-strain plot.


(e)  The ductility, in percent elongation, is just the plastic strain at fracture, multiplied by one-hundred.  The total fracture strain at fracture is 0.165;  subtracting out the elastic strain (which is about 0.005) leaves a plastic strain of 0.160.  Thus, the ductility is about 16%EL.


(f)  From Equation 6.14, the modulus of resilience is just


[image: image137.wmf]
which, using data computed above gives a value of


[image: image138.wmf]

6.30  A specimen of ductile cast iron having a rectangular cross section of dimensions 4.8 mm ( 15.9 mm (3/16 in. ( 5/8 in.) is deformed in tension.  Using the load-elongation data tabulated below, complete problems (a) through (f).

	Load
	Length

	N
	lbf
	mm
	in.

	0
	0
	75.000
	2.953

	4,740
	1,065
	75.025
	2.954

	9,140
	2,055
	75.050
	2.955

	12,920
	2,900
	75.075
	2.956

	16,540
	3,720
	75.113
	2.957

	18,300
	4,110
	75.150
	2.959

	20,170
	4,530
	75.225
	2.962

	22,900
	5,145
	75.375
	2.968

	25,070
	5,635
	75.525
	2.973

	26,800
	6,025
	75.750
	2.982

	28,640
	6,440
	76.500
	3.012

	30,240
	6,800
	78.000
	3.071

	31,100
	7,000
	79.500
	3.130

	31,280
	7,030
	81.000
	3.189

	30,820
	6,930
	82.500
	3.248

	29,180
	6,560
	84.000
	3.307

	27,190
	6,110
	85.500
	3.366

	24,140
	5,430
	87.000
	3.425

	18,970
	4,265
	88.725
	3.493

	Fracture



(a) Plot the data as engineering stress versus engineering strain.


(b) Compute the modulus of elasticity.


(c) Determine the yield strength at a strain offset of 0.002.


(d) Determine the tensile strength of this alloy.


(e) Compute the modulus of resilience.


(f) What is the ductility, in percent elongation?



Solution

This problem calls for us to make a stress-strain plot for a ductile cast iron, given its tensile load-length data, and then to determine some of its mechanical characteristics.


(a)  The data are plotted below on two plots:  the first corresponds to the entire stress-strain curve, while for the second, the curve extends just beyond the elastic region of deformation.

[image: image139.png]0.2

0.1
Strain

1

o o
S o
) Al

(BdN) SS211S

400

100 |

0.0




[image: image140.png]Stress (MPa)

300

200

100

0
0.000

0.001

0.002

0.003

Strain

0.004

0.005

0.006





(b)  The elastic modulus is the slope in the linear elastic region (Equation 6.10) as


[image: image141.wmf]

(c)  For the yield strength, the 0.002 strain offset line is drawn dashed.  It intersects the stress-strain curve at approximately 280 MPa (40,500 psi).


(d)  The tensile strength is approximately 410 MPa (59,500 psi), corresponding to the maximum stress on the complete stress-strain plot.


(e)  From Equation 6.14, the modulus of resilience is just


[image: image142.wmf]
which, using data computed above, yields a value of


[image: image143.wmf]

(f)  The ductility, in percent elongation, is just the plastic strain at fracture, multiplied by one-hundred.  The total fracture strain at fracture is 0.185;  subtracting out the elastic strain (which is about 0.001) leaves a plastic strain of 0.184.  Thus, the ductility is about 18.4%EL.


6.31  For the titanium alloy, whose stress strain behavior may be observed in the “Tensile Tests” module of Virtual Materials Science and Engineering (VMSE), determine the following:


(a) the approximate yield strength (0.002 strain offset),


(b) the tensile strength, and


(c) the approximate ductility, in percent elongation.

How do these values compare with those for the two Ti-6Al-4V alloys presented in Table B.4 of Appendix B?


Solution

(a)  It is possible to do a screen capture and then print out the entire stress-strain curve for the Ti alloy.  The intersection of a straight line parallel to the initial linear region of the curve and offset at a strain of 0.002 with this curve is at approximately 720 MPa.


(b)  The maximum reading in the stress window located below the plot as the curser point is dragged along the stress-strain curve is 1000 MPa, the value of the tensile strength.


(c)  The approximate percent elongation corresponds to the strain at fracture multiplied by 100 (i.e., 12%) minus the maximum elastic strain (i.e., value of strain at which the linearity of the curve ends multiplied by 100—in this case about 0.5%);  this gives a value of about 11.5%EL.


From Table B.4 in Appendix B, yield strength, tensile strength, and percent elongation values for the anneal Ti-6Al-4V are 830 MPa, 900 MPa, and 14%EL, while for the solution heat treated and aged alloy, the corresponding values are 1103 MPa, 1172 MPa, and 10%EL.  Thus, tensile strength and percent elongation values for the VMSE alloy are slightly lower than for the annealed material in Table B.4 (720 vs 830 MPa, and 11.5 vs. 14 %EL), whereas the tensile strength is slightly higher (1000 vs. 900 MPa).

6.32  For the tempered steel alloy, whose stress strain behavior may be observed in the “Tensile Tests” module of Virtual Materials Science and Engineering (VMSE), determine the following:


(a) the approximate yield strength (0.002 strain offset),


(b) the tensile strength, and


(c) the approximate ductility, in percent elongation.

How do these values compare with those for the oil-quenched and tempered 4140 and 4340 steel alloys presented in Table B.4 of Appendix B?



Solution

(a)  It is possible to do a screen capture and then print out the entire stress-strain curve for the tempered steel alloy.  The intersection of a straight line parallel to the initial linear region of the curve and offset at a strain of 0.002 with this curve is at approximately 1430 MPa.


(b)  The maximum reading in the stress window located below the plot as the curser point is dragged along the stress-strain curve is 1656 MPa, the value of the tensile strength.


(c)  The approximate percent elongation corresponds to the strain at fracture multiplied by 100 (i.e., 14.8%) minus the maximum elastic strain (i.e., value of strain at which the linearity of the curve ends multiplied by 100—in this case about 0.8%);  this gives a value of about 14.0%EL.


For the oil-quenched and tempered 4140 and 4340 steel alloys, yield strength values presented in Table B.4 of Appendix B are 1570 MPa and 1620 MPa, respectively;  these values are somewhat larger than the 1430 MPa for the tempered steel alloy of VMSE.  Tensile strength values for these 4140 and 4340 alloys are, respectively 1720 MPa and 1760 MPa (compared to 1656 MPa for the VMSE steel).  And, finally, the respective ductilities for the 4140 and 4340 alloys are 11.5%EL and 12%EL, which are slightly lower than the 14%EL value for the VMSE steel.

6.33  For the aluminum alloy, whose stress strain behavior may be observed in the “Tensile Tests” module of Virtual Materials Science and Engineering (VMSE), determine the following:


(a) the approximate yield strength (0.002 strain offset),


(b) the tensile strength, and


(c) the approximate ductility, in percent elongation.

How do these values compare with those for the 2024 aluminum alloy (T351 temper) presented in Table B.4 of Appendix B?


Solution

(a)  It is possible to do a screen capture and then print out the entire stress-strain curve for the aluminum alloy.  The intersection of a straight line parallel to the initial linear region of the curve and offset at a strain of 0.002 with this curve is at approximately 300 MPa.


(b)  The maximum reading in the stress window located below the plot as the curser point is dragged along the stress-strain curve is 484 MPa, the value of the tensile strength.


(c)  The approximate percent elongation corresponds to the strain at fracture multiplied by 100 (i.e., 22.4%) minus the maximum elastic strain (i.e., value of strain at which the linearity of the curve ends multiplied by 100—in this case about 0.5%);  this gives a value of about 21.9%EL.


For the 2024 aluminum alloy (T351 temper), the yield strength value presented in Table B.4 of Appendix B is 325, which is slightly larger than the 300 MPa for the aluminum alloy of VMSE.  The tensile strength value for the 2024-T351 is 470 MPa (compared to 484 MPa for the VMSE alloy).  And, finally, the ductility for 2024-T351 is  20%EL, which is about the same as for the VMSE aluminum (21.9%EL).

6.34  For the (plain) carbon steel alloy, whose stress strain behavior may be observed in the “Tensile Tests” module of Virtual Materials Science and Engineering (VMSE), determine the following:


(a) the approximate yield strength,


(b) the tensile strength, and


(c) the approximate ductility, in percent elongation.



Solution

(a)  It is possible to do a screen capture and then print out the entire stress-strain curve for the plain carbon steel alloy.  Inasmuch as the stress-strain curve displays the yield point phenomenon, we take the yield strength as the lower yield point, which, for this steel, is about 225 MPa.


(b)  The maximum reading in the stress window located below the plot as the curser point is dragged along the stress-strain curve is 274 MPa, the value of the tensile strength.


(c)  The approximate percent elongation corresponds to the strain at fracture multiplied by 100 (i.e., 43.0%) minus the maximum elastic strain (i.e., value of strain at which the linearity of the curve ends multiplied by 100—in this case about 0.6%);  this gives a value of about 42.4%EL.


6.35  A cylindrical metal specimen having an original diameter of 12.8 mm (0.505 in.) and gauge length of 50.80 mm (2.000 in.) is pulled in tension until fracture occurs.  The diameter at the point of fracture is 6.60 mm (0.260 in.), and the fractured gauge length is 72.14 mm (2.840 in.).  Calculate the ductility in terms of percent reduction in area and percent elongation.


Solution

This problem calls for the computation of ductility in both percent reduction in area and percent elongation.  Percent reduction in area is computed using Equation 6.12 as


[image: image144.wmf]
in which d0 and df  are, respectively, the original and fracture cross-sectional areas.  Thus,


[image: image145.wmf]
While, for percent elongation, we use Equation 6.11 as


[image: image146.wmf]

[image: image147.wmf]

6.36  Calculate the moduli of resilience for the materials having the stress–strain behaviors shown in Figures 6.12 and 6.21.


Solution

This problem asks us to calculate the moduli of resilience for the materials having the stress-strain behaviors shown in Figures 6.12 and 6.21.  According to Equation 6.14, the modulus of resilience Ur is a function of the yield strength and the modulus of elasticity as


[image: image148.wmf]
The values for y and E for the brass in Figure 6.12 are determined in Example Problem 6.3 as 250 MPa (36,000 psi) and 93.8 GPa (13.6 ( 106 psi), respectively.  Thus


[image: image149.wmf]

Values of the corresponding parameters for the steel alloy (Figure 6.21) are determined in Problem 6.25 as 400 MPa (58,000 psi) and 200 GPa (29 ( 106 psi), respectively, and therefore


[image: image150.wmf]

6.37  Determine the modulus of resilience for each of the following alloys:

	
	Yield Strength

	Material
	MPa
	psi

	Steel alloy
	550
	80,000

	Brass alloy
	350
	50,750

	Aluminum alloy
	250
	36,250

	Titanium alloy
	800
	116,000


Use modulus of elasticity values in Table 6.1.


Solution

The moduli of resilience of the alloys listed in the table may be determined using Equation 6.14.  Yield strength values are provided in this table, whereas the elastic moduli are tabulated in Table 6.1.


For steel


[image: image151.wmf]

[image: image152.wmf]

For the brass


[image: image153.wmf]

For the aluminum alloy


[image: image154.wmf]

And, for the titanium alloy


[image: image155.wmf]

6.38 A brass alloy to be used for a spring application must have a modulus of resilience of at least 0.75 MPa (110 psi). What must be its minimum yield strength?


Solution

The modulus of resilience, yield strength, and elastic modulus of elasticity are related to one another through Equation 6.14;  the value of E for brass given in Table 6.1 is 97 GPa.  Solving for y from this expression yields


[image: image156.wmf]
= 381 MPa  (55,500 psi)


True Stress and Strain

6.39  Show that Equations 6.18a and 6.18b are valid when there is no volume change during deformation.


Solution

To show that Equation 6.18a is valid, we must first rearrange Equation 6.17 as


[image: image157.wmf]
Substituting this expression into Equation 6.15 yields


[image: image158.wmf]
But, from Equation 6.2


[image: image159.wmf]
Or


[image: image160.wmf]
Thus,


[image: image161.wmf]

For Equation 6.18b


[image: image162.wmf]
is valid since, from Equation 6.16


[image: image163.wmf]
and


[image: image164.wmf]
from above.


6.40 Demonstrate that Equation 6.16, the expression defining true strain, may also be represented by
∈T = ln 
[image: image165.wmf]
when specimen volume remains constant during deformation. Which of these two expressions is more valid during necking? Why?


Solution

This problem asks us to demonstrate that true strain may also be represented by

∈T = ln 
[image: image166.wmf]
Rearrangement of Equation 6.17 leads to


[image: image167.wmf]
Thus, Equation 6.16 takes the form

∈T 
[image: image168.wmf]

The expression ∈T = ln 
[image: image169.wmf] is more valid during necking because Ai is taken as the area of the neck. 


6.41  Using the data in Problem 6.28 and Equations 6.15, 6.16, and 6.18a, generate a true stress–true strain plot for aluminum. Equation 6.18a becomes invalid past the point at which necking begins; therefore, measured diameters are given below for the last four data points, which should be used in true stress computations.
	Load
	Length
	Diameter

	N
	lbf
	mm
	in.
	mm
	in.

	46,100
	10,400
	56.896
	2.240
	11.71
	0.461

	42,400
	10,100
	57.658
	2.270
	10.95
	0.431

	42,600
	9,600
	58.420
	2.300
	10.62
	0.418

	36,400
	8,200
	59.182
	2.330
	9.40
	0.370




Solution

These true stress-strain data are plotted below.

[image: image170.png]0.1
True strain

500 -

400 -

1 1
S S
S =3
en (@]

(BdIN) $S3.s dnu ],

0.0

100





6.42  A tensile test is performed on a metal specimen, and it is found that a true plastic strain of 0.20 is produced when a true stress of 575 MPa (83,500 psi) is applied; for the same metal, the value of K in Equation 6.19 is 860 MPa (125,000 psi).  Calculate the true strain that results from the application of a true stress of 600 MPa (87,000 psi).


Solution

It first becomes necessary to solve for n in Equation 6.19.  Taking logarithms of this expression and after rearrangement we have


[image: image171.wmf]
And, incorporating values of the parameters provided in the problem statement leads to


[image: image172.wmf]
Expressing T as the dependent variable (Equation 6.19), and then solving for its value from the data stipulated in the problem statement, leads to


[image: image173.wmf]

6.43  For some metal alloy, a true stress of 415 MPa (60,175 psi) produces a plastic true strain of 0.475.  How much will a specimen of this material elongate when a true stress of 325 MPa (46,125 psi) is applied if the original length is 300 mm (11.8 in.)?  Assume a value of 0.25 for the strain-hardening exponent n.


Solution

Solution of this problem requires that we utilize Equation 6.19.  It is first necessary to solve for K from the given true stress and strain.  Rearrangement of this equation yields


[image: image174.wmf]
Next we must solve for the true strain produced when a true stress of 325 MPa is applied, also using Equation 6.19.  Thus


[image: image175.wmf]
Now, solving for li gives


[image: image176.wmf]
And finally, the elongation ∆l is just


[image: image177.wmf]

6.44  The following true stresses produce the corresponding true plastic strains for a brass alloy:

	True Stress (psi)
	True Strain

	50,000
	0.10

	60,000
	0.20


What true stress is necessary to produce a true plastic strain of 0.25?



Solution

For this problem, we are given two values of T and T, from which we are asked to calculate the true stress which produces a true plastic strain of 0.25.  Employing Equation 6.19, we may set up two simultaneous equations with two unknowns (the unknowns being K and n), as


[image: image178.wmf]

[image: image179.wmf]
Solving for n from these two expressions yields


[image: image180.wmf]
and for K

log K = 4.96 or K = 104.96 =  91,623 psi

Thus, for T = 0.25


[image: image181.wmf]

6.45  For a brass alloy, the following engineering stresses produce the corresponding plastic engineering strains, prior to necking:
	Engineering Stress (MPa)
	Engineering Strain

	235
	0.194

	250
	0.296


On the basis of this information, compute the engineering stress necessary to produce an engineering strain of 0.25.


Solution

For this problem we first need to convert engineering stresses and strains to true stresses and strains so that the constants K and n in Equation 6.19 may be determined.  Since T = (1 + ) then


[image: image182.wmf]

[image: image183.wmf]
Similarly for strains, since T = ln(1 + ) then


[image: image184.wmf]

[image: image185.wmf]
Taking logarithms of Equation 6.19, we get


[image: image186.wmf]
which allows us to set up two simultaneous equations for the above pairs of true stresses and true strains, with K and n as unknowns.  Thus


[image: image187.wmf]

[image: image188.wmf]
Solving for these two expressions yields K = 543 MPa and n = 0.383.


Now, converting  = 0.25 to true strain


[image: image189.wmf]
The corresponding T to give this value of T (using Equation 6.19) is just


[image: image190.wmf]
Now converting this value of T to an engineering stress using Equation 6.18a gives


[image: image191.wmf]

6.46 Find the toughness (or energy to cause fracture) for a metal that experiences both elastic and plastic deformation.  Assume Equation 6.5 for elastic deformation, that the modulus of elasticity is 172 GPa (25 ( 106 psi), and that elastic deformation terminates at a strain of 0.01.  For plastic deformation, assume that the relationship between stress and strain is described by Equation 6.19, in which the values for K and n are 6900 MPa (1 ( 106 psi) and 0.30, respectively. Furthermore, plastic deformation occurs between strain values of 0.01 and 0.75, at which point fracture occurs.


Solution

This problem calls for us to compute the toughness (or energy to cause fracture).  The easiest way to do this is to integrate both elastic and plastic regions, and then add them together.


[image: image192.wmf]

[image: image193.wmf]

[image: image194.wmf]

[image: image195.wmf]
=  3.65 ( 109 J/m3  (5.29 ( 105 in.-lbf/in.3)


6.47  For a tensile test, it can be demonstrated that necking begins when



[image: image196.wmf]
(6.26)

Using Equation 6.19, determine the value of the true strain at this onset of necking.


Solution

Let us take the derivative of Equation 6.19, set it equal to T, and then solve for T from the resulting expression.  Thus


[image: image197.wmf]
However, from Equation 6.19, T = K(T)n, which, when substituted into the above expression, yields


[image: image198.wmf]
Now solving for T from this equation leads to

T = n
as the value of the true strain at the onset of necking.


6.48 Taking the logarithm of both sides of Equation 6.19 yields

log σT = log K + n log ∈T
(6.27)
Thus, a plot of log σT versus log ∈T in the plastic region to the point of necking should yield a straight line having a slope of n and an intercept (at log σT = 0) of log K.


Using the appropriate data tabulated in Problem 6.29, make a plot of log σT versus log ∈T and determine the values of n and K. It will be necessary to convert engineering stresses and strains to true stresses and strains using Equations 6.18a and 6.18b.



Solution

This problem calls for us to utilize the appropriate data from Problem 6.29 in order to determine the values of n and K for this material.  From Equation 6.27 the slope and intercept of a log T versus log T plot will yield n and log K, respectively.  However, Equation 6.19 is only valid in the region of plastic deformation to the point of necking;  thus, only the 7th, 8th, 9th, and 10th data points may be utilized.  The log-log plot with these data points is given below.

[image: image199.png]-1.2

1.4

-1.6

-1.8

-2.0

2.60

258 I

1
o
o

1 1 |

© < Ql

0 o) o]

ai ai ai ai

(edJN) $S9.3s ana) 3o0[

248 I

2.46
-2.2

log true strain




The slope yields a value of 0.136 for n, whereas the intercept gives a value of 2.7497 for log K, and thus K = 102.7497 = 562 MPa.


Elastic Recovery After Plastic Deformation

6.49  A cylindrical specimen of a brass alloy 7.5 mm (0.30 in.) in diameter and 90.0 mm (3.54 in.) long is pulled in tension with a force of 6000 N (1350 lbf);  the force is subsequently released.

(a) Compute the final length of the specimen at this time. The tensile stress–strain behavior for this alloy is shown in Figure 6.12.


(b) Compute the final specimen length when the load is increased to 16,500 N (3700 lbf) and then released.


Solution

(a)  In order to determine the final length of the brass specimen when the load is released, it first becomes necessary to compute the applied stress using Equation 6.1;  thus


[image: image200.wmf]
Upon locating this point on the stress-strain curve (Figure 6.12), we note that it is in the linear, elastic region;  therefore, when the load is released the specimen will return to its original length of 90 mm (3.54 in.).


(b)  In this portion of the problem we are asked to calculate the final length, after load release, when the load is increased to 16,500 N (3700 lbf).  Again, computing the stress


[image: image201.wmf]
The point on the stress-strain curve corresponding to this stress is in the plastic region.  We are able to estimate the amount of permanent strain by drawing a straight line parallel to the linear elastic region;  this line intersects the strain axis at a strain of about 0.08 which is the amount of plastic strain.  The final specimen length li may be determined from a rearranged form of Equation 6.2 as

li = l0(1 + ) = (90 mm)(1 + 0.08) = 97.20 mm (3.82 in.)


6.50  A steel alloy specimen having a rectangular cross section of dimensions 12.7 mm × 6.4 mm (0.5 in. × 0.25 in.) has the stress–strain behavior shown in Figure 6.21. If this specimen is subjected to a tensile force of 38,000 N (8540 lbf) then


(a) Determine the elastic and plastic strain values.


(b) If its original length is 460 mm (18.0 in.), what will be its final length after the load in part (a) is applied and then released?



Solution

(a)  We are asked to determine both the elastic and plastic strain values when a tensile force of 38,000 N (8540 lbf) is applied to the steel specimen and then released.  First it becomes necessary to determine the applied stress using Equation 6.1;  thus


[image: image202.wmf]
where b0 and d0 are cross-sectional width and depth (12.7 mm and 6.4 mm, respectively).  Thus


[image: image203.wmf]
From Figure 6.21, this point is in the plastic region so the specimen will be both elastic and plastic strains.  The total strain at this point, t, is about 0.010.  We are able to estimate the amount of permanent strain recovery e from Hooke's law, Equation 6.5 as


[image: image204.wmf]
And, since E = 207 GPa for steel (Table 6.1)


[image: image205.wmf]
The value of the plastic strain, p is just the difference between the total and elastic strains;  that is

p = t – e = 0.010 – 0.00226 = 0.00774


(b)  If the initial length is 460 mm (18.0 in.) then the final specimen length li may be determined from a rearranged form of Equation 6.2 using the plastic strain value as

li = l0(1 + p) = (460 mm)(1 + 0.00774) = 463.6 mm (18.14 in.)


Hardness

6.51  (a) A 10-mm-diameter Brinell hardness indenter produced an indentation 1.62 mm in diameter in a steel alloy when a load of 500 kg was used. Compute the HB of this material.

(b) What will be the diameter of an indentation to yield a hardness of 450 HB when a 500 kg load is used?


Solution

(a)  We are asked to compute the Brinell hardness for the given indentation.  It is necessary to use the equation in Table 6.5 for HB, where P = 500 kg, d = 1.62 mm, and D = 10 mm.  Thus, the Brinell hardness is computed as


[image: image206.wmf]

[image: image207.wmf]

(b)  This part of the problem calls for us to determine the indentation diameter d which will yield a 450 HB when P = 500 kg.  Solving for d from the equation in Table 6.5 gives


[image: image208.wmf]

[image: image209.wmf]

6.52  Estimate the Brinell and Rockwell hardnesses for the following:


(a) The naval brass for which the stress–strain behavior is shown in Figure 6.12.


(b) The steel alloy for which the stress–strain behavior is shown in Figure 6.21.


Solution

This problem calls for estimations of Brinell and Rockwell hardnesses.


(a)  For the brass specimen, the stress-strain behavior for which is shown in Figure 6.12, the tensile strength is 450 MPa (65,000 psi).  From Figure 6.19, the hardness for brass corresponding to this tensile strength is about 125 HB or 70 HRB.


(b)  The steel alloy (Figure 6.21) has a tensile strength of about 515 MPa (74,700 psi) [Problem 6.25(d)].  This corresponds to a hardness of about 160 HB or ~90 HRB from the line for steels in Figure 6.19.  Alternately, using Equation 6.20a


[image: image210.wmf]

6.53  Using the data represented in Figure 6.19, specify equations relating tensile strength and Brinell hardness for brass and nodular cast iron, similar to Equations 6.20a and 6.20b for steels.


Solution

These equations, for a straight line, are of the form

TS = C + (E)(HB)

where TS is the tensile strength, HB is the Brinell hardness, and C and E are constants, which need to be determined.


One way to solve for C and E is analytically--establishing two equations using TS and HB data points on the plot, as

(TS)1 = C + (E)(BH)1
(TS)2 = C + (E)(BH)2
Solving for E from these two expressions yields


[image: image211.wmf]
For nodular cast iron, if we make the arbitrary choice of (HB)1 and (HB)2 as 200 and 300, respectively, then, from Figure 6.19, (TS)1 and (TS)2 take on values of 600 MPa (87,000 psi) and 1100 MPa (160,000 psi), respectively.  Substituting these values into the above expression and solving for E gives


[image: image212.wmf]
Now, solving for C yields

C = (TS)1 – (E)(BH)1
= 600 MPa - (5.0 MPa/HB)(200 HB) = – 400 MPa (– 59,000 psi)

Thus, for nodular cast iron, these two equations take the form

TS(MPa) = – 400 + 5.0 x HB

TS(psi) = – 59,000 + 730 x HB


Now for brass, we take (HB)1 and (HB)2 as 100 and 200, respectively, then, from Figure 7.31, (TS)1 and (TS)2 take on values of 370 MPa (54,000 psi) and 660 MPa (95,000 psi), respectively.  Substituting these values into the above expression and solving for E gives


[image: image213.wmf]
Now, solving for C yields

C = (TS)1 – (E)(BH)1
= 370 MPa – (2.9 MPa/HB)(100 HB) = 80 MPa  (13,000 psi)

Thus, for brass these two equations take the form

TS(MPa) = 80 + 2.9 x HB

TS(psi) = 13,000 + 410 x HB


Variability of Material Properties

6.54  Cite five factors that lead to scatter in measured material properties.


Solution

The five factors that lead to scatter in measured material properties are the following:  (1) test method;  (2) variation in specimen fabrication procedure;  (3) operator bias;  (4) apparatus calibration;  and (5) material inhomogeneities and/or compositional differences.


6.55  Below are tabulated a number of Rockwell B hardness values that were measured on a single steel specimen. Compute average and standard deviation hardness values.

	83.3
	80.7
	86.4

	88.3
	84.7
	85.2

	82.8
	87.8
	86.9

	86.2
	83.5
	84.4

	87.2
	85.5
	86.3




Solution

The average of the given hardness values is calculated using Equation 6.21 as


[image: image214.wmf]

[image: image215.wmf]

And we compute the standard deviation using Equation 6.22 as follows:


[image: image216.wmf]

[image: image217.wmf]

[image: image218.wmf]

Design/Safety Factors

6.56  Upon what three criteria are factors of safety based?


Solution

The criteria upon which factors of safety are based are (1) consequences of failure, (2) previous experience, (3) accuracy of measurement of mechanical forces and/or material properties, and (4) economics.


6.57  Determine working stresses for the two alloys that have the stress–strain behaviors shown in Figures 6.12 and 6.21.


Solution

The working stresses for the two alloys the stress-strain behaviors of which are shown in Figures 6.12 and 6.21 are calculated by dividing the yield strength by a factor of safety, which we will take to be 2.  For the brass alloy (Figure 6.12), since y = 250 MPa (36,000 psi), the working stress is 125 MPa (18,000 psi), whereas for the steel alloy (Figure 6.21), y = 400 MPa (58,000 psi), and, therefore, w = 200 MPa (29,000 psi).

DESIGN PROBLEMS


6.D1  A large tower is to be supported by a series of steel wires.  It is estimated that the load on each wire will be 11,100 N (2500 lbf).  Determine the minimum required wire diameter assuming a factor of safety of 2 and a yield strength of 1030 MPa (150,000 psi).


Solution

For this problem the working stress is computed using Equation 6.24 with N = 2, as


[image: image219.wmf]
Since the force is given, the area may be determined from Equation 6.1, and subsequently the original diameter d0 may be calculated as


[image: image220.wmf]
And


[image: image221.wmf]
= 5.23 ( 10-3 m = 5.23 mm (0.206 in.)


6.D2  (a) Gaseous hydrogen at a constant pressure of 1.013 MPa (10 atm) is to flow within the inside of a thin-walled cylindrical tube of nickel that has a radius of 0.1 m.  The temperature of the tube is to be 300(C and the pressure of hydrogen outside of the tube will be maintained at 0.01013 MPa (0.1 atm). Calculate the minimum wall thickness if the diffusion flux is to be no greater than 1 ( 10-7 mol/m2-s.  The concentration of hydrogen in the nickel, CH (in moles hydrogen per m3 of Ni) is a function of hydrogen pressure, PH2 (in MPa) and absolute temperature (T) according to


[image: image222.wmf]
(6.28)

Furthermore, the diffusion coefficient for the diffusion of H in Ni depends on temperature as


[image: image223.wmf]
(6.29)


(b) For thin-walled cylindrical tubes that are pressurized, the circumferential stress is a function of the pressure difference across the wall (Δp), cylinder radius (r), and tube thickness (Δx) as



[image: image224.wmf]
(6.30)

Compute the circumferential stress to which the walls of this pressurized cylinder are exposed.


(c) The room-temperature yield strength of Ni is 100 MPa (15,000 psi) and, furthermore, sy diminishes about 5 MPa for every 50(C rise in temperature. Would you expect the wall thickness computed in part (b) to be suitable for this Ni cylinder at 300(C?  Why or why not?


(d) If this thickness is found to be suitable, compute the minimum thickness that could be used without any deformation of the tube walls. How much would the diffusion flux increase with this reduction in thickness? On the other hand, if the thickness determined in part (c) is found to be unsuitable, then specify a minimum thickness that you would use. In this case, how much of a diminishment in diffusion flux would result?


Solution

(a)  This portion of the problem asks for us to compute the wall thickness of a thin-walled cylindrical Ni tube at 300C through which hydrogen gas diffuses.  The inside and outside pressures are, respectively, 1.1013 and 0.01013 MPa, and the diffusion flux is to be no greater than 1 ( 10-7 mol/m2-s.  This is a steady-state diffusion problem, which necessitates that we employ Equation 5.3.  The concentrations at the inside and outside wall faces may be determined using Equation 6.28, and, furthermore, the diffusion coefficient is computed using Equation 6.29.  Solving for x (using Equation 5.3)

[image: image225.wmf]

[image: image226.wmf]

[image: image227.wmf]

[image: image228.wmf]
= 0.0025 m = 2.5 mm


(b)  Now we are asked to determine the circumferential stress:


[image: image229.wmf]

[image: image230.wmf]
= 10.0 MPa


(c)  Now we are to compare this value of stress to the yield strength of Ni at 300C, from which it is possible to determine whether or not the 2.5 mm wall thickness is suitable.  From the information given in the problem, we may write an equation for the dependence of yield strength (y) on temperature (T) as follows:


[image: image231.wmf]
where Tr is room temperature and for temperature in degrees Celsius.  Thus, at 300C


[image: image232.wmf]
Inasmuch as the circumferential stress (10 MPa) is much less than the yield strength (72 MPa), this thickness is entirely suitable.


(d)  And, finally, this part of the problem asks that we specify how much this thickness may be reduced and still retain a safe design.  Let us use a working stress by dividing the yield stress by a factor of safety, according to Equation 6.24.  On the basis of our experience, let us use a value of 2.0 for N.  Thus


[image: image233.wmf]
Using this value for w and Equation 6.30, we now compute the tube thickness as


[image: image234.wmf]

[image: image235.wmf]
= 0.00070 m = 0.70 mm

Substitution of this value into Fick's first law we calculate the diffusion flux as follows:


[image: image236.wmf]

[image: image237.wmf]

[image: image238.wmf]
= 3.53 ( 10-7 mol/m2-s

Thus, the flux increases by approximately a factor of 3.5, from 1 ( 10-7 to 3.53 ( 10-7 mol/m2-s with this reduction in thickness.


6.D3  Consider the steady-state diffusion of hydrogen through the walls of a cylindrical nickel tube as described in Problem 6.D2.  One design calls for a diffusion flux of 5 ( 10-8 mol/m2-s, a tube radius of 0.125 m, and inside and outside pressures of 2.026 MPa (20 atm) and 0.0203 MPa (0.2 atm), respectively;  the maximum allowable temperature is 450(C.  Specify a suitable temperature and wall thickness to give this diffusion flux and yet ensure that the tube walls will not experience any permanent deformation.



Solution

This problem calls for the specification of a temperature and cylindrical tube wall thickness that will give a diffusion flux of 5 ( 10-8 mol/m2-s for the diffusion of hydrogen in nickel;  the tube radius is 0.125 m and the inside and outside pressures are 2.026 and 0.0203 MPa, respectively.  There are probably several different approaches that may be used;  and, of course, there is not one unique solution.  Let us employ the following procedure to solve this problem:  (1)  assume some wall thickness, and, then, using Fick's first law for diffusion (which also employs Equations 5.3 and 6.29), compute the temperature at which the diffusion flux is that required;  (2)  compute the yield strength of the nickel at this temperature using the dependence of yield strength on temperature as stated in Problem 6.D2;  (3)  calculate the circumferential stress on the tube walls using Equation 6.30;  and (4)  compare the yield strength and circumferential stress values--the yield strength should probably be at least twice the stress in order to make certain that no permanent deformation occurs.  If this condition is not met then another iteration of the procedure should be conducted with a more educated choice of wall thickness.


As a starting point, let us arbitrarily choose a wall thickness of 2 mm (2 ( 10-3 m).  The steady-state diffusion equation, Equation 5.3, takes the form


[image: image239.wmf]
= 5 ( 10-8 mol/m2-s


[image: image240.wmf]

[image: image241.wmf]
Solving this expression for the temperature T gives T = 514 K = 241C;  this value is satisfactory inasmuch as it is less than the maximum allowable value (450C).


The next step is to compute the stress on the wall using Equation 6.30;  thus


[image: image242.wmf]

[image: image243.wmf]
= 31.3 MPa

Now, the yield strength (y) of Ni at this temperature may be computed using the expression


[image: image244.wmf]
where Tr is room temperature.  Thus,
y = 100 MPa – (0.1 MPa/(C)(241C – 20C) = 77.9 MPa

Inasmuch as this yield strength is greater than twice the circumferential stress, wall thickness and temperature values of 2 mm and 241C are satisfactory design parameters.










PAGE  
Excerpts from this work may be reproduced by instructors for distribution on a not-for-profit basis for testing or instructional purposes only to students enrolled in courses for which the textbook has been adopted.  Any other reproduction or translation of this work beyond that permitted by Sections 107 or 108 of the 1976 United States Copyright Act without the permission of the copyright owner is unlawful.

_1073495051.unknown

_1175778501.unknown

_1175847223.unknown

_1179217905.unknown

_1179255588.unknown

_1179256008.unknown

_1179257319.unknown

_1179305469.unknown

_1179305882.unknown

_1179306625.unknown

_1179306662.unknown

_1179305957.unknown

_1179305638.unknown

_1179257673.unknown

_1179256547.unknown

_1179257198.unknown

_1179256329.unknown

_1179255663.unknown

_1179255833.unknown

_1179255646.unknown

_1179234121.unknown

_1179255237.unknown

_1179255408.unknown

_1179255212.unknown

_1179220613.unknown

_1179233579.unknown

_1179219868.unknown

_1175849394.unknown

_1175850695.unknown

_1175853143.unknown

_1175853361.unknown

_1175853997.unknown

_1175854055.unknown

_1175854215.unknown

_1175853437.unknown

_1175853215.unknown

_1175852808.unknown

_1175853062.unknown

_1175850744.unknown

_1175849934.unknown

_1175850663.unknown

_1175849730.unknown

_1175848706.unknown

_1175848837.unknown

_1175849285.unknown

_1175848743.unknown

_1175848575.unknown

_1175848626.unknown

_1175848061.unknown

_1175842848.unknown

_1175844103.unknown

_1175844535.unknown

_1175846350.unknown

_1175846508.unknown

_1175844759.unknown

_1175844217.unknown

_1175844278.unknown

_1175844160.unknown

_1175843923.unknown

_1175844009.unknown

_1175844083.unknown

_1175843983.unknown

_1175843096.unknown

_1175843873.unknown

_1175842868.unknown

_1175780212.unknown

_1175800426.unknown

_1175801016.unknown

_1175801124.unknown

_1175800956.unknown

_1175796814.unknown

_1175800271.unknown

_1175796629.unknown

_1175779166.unknown

_1175779968.unknown

_1175780140.unknown

_1175779676.unknown

_1175778925.unknown

_1175778945.unknown

_1175778856.unknown

_1175760861.unknown

_1175765023.unknown

_1175768022.unknown

_1175773108.unknown

_1175776510.unknown

_1175778348.unknown

_1175773260.unknown

_1175772299.unknown

_1175772424.unknown

_1175768133.unknown

_1175766923.unknown

_1175767507.unknown

_1175767857.unknown

_1175767215.unknown

_1175766435.unknown

_1175766532.unknown

_1175765058.unknown

_1175763853.unknown

_1175764871.unknown

_1175764959.unknown

_1175764991.unknown

_1175764906.unknown

_1175764127.unknown

_1175764277.unknown

_1175763932.unknown

_1175761318.unknown

_1175761971.unknown

_1175762035.unknown

_1175761644.unknown

_1175761135.unknown

_1175761231.unknown

_1175761012.unknown

_1175712472.unknown

_1175758431.unknown

_1175759459.unknown

_1175760128.unknown

_1175760514.unknown

_1175759866.unknown

_1175759068.unknown

_1175759251.unknown

_1175758579.unknown

_1175757857.unknown

_1175757936.unknown

_1175758315.unknown

_1175757892.unknown

_1175715506.unknown

_1175757831.unknown

_1175715352.unknown

_1175709688.unknown

_1175710576.unknown

_1175710880.unknown

_1175710899.unknown

_1175710770.unknown

_1175710108.unknown

_1175710129.unknown

_1175710063.unknown

_1116322482.unknown

_1126116132.unknown

_1169577895.unknown

_1174506268.unknown

_1175709374.unknown

_1174505068.unknown

_1169577757.unknown

_1126427801.unknown

_1116323557.unknown

_1116323760.unknown

_1116323992.unknown

_1116322507.unknown

_1073495997.unknown

_1073497663.unknown

_1073544025.unknown

_1073544716.unknown

_1073543712.unknown

_1073496443.unknown

_1073495140.unknown

_1072536109.unknown

_1072538026.unknown

_1072612669.unknown

_1072617009.unknown

_1072618447.unknown

_1072618672.unknown

_1072619092.unknown

_1072619159.unknown

_1072619193.unknown

_1072618692.unknown

_1072618518.unknown

_1072617641.unknown

_1072618278.unknown

_1072617355.unknown

_1072614916.unknown

_1072615546.unknown

_1072616905.unknown

_1072615527.unknown

_1072612754.unknown

_1072614202.unknown

_1072612700.unknown

_1072553999.unknown

_1072612599.unknown

_1072612644.unknown

_1072612655.unknown

_1072612634.unknown

_1072612148.unknown

_1072612425.unknown

_1072554632.unknown

_1072545062.unknown

_1072546285.unknown

_1072546454.unknown

_1072545072.unknown

_1072538074.unknown

_1072538096.unknown

_1072538064.unknown

_1072536790.unknown

_1072537077.unknown

_1072537985.unknown

_1072537998.unknown

_1072537103.unknown

_1072536975.unknown

_1072537047.unknown

_1072536814.unknown

_1072536559.unknown

_1072536585.unknown

_1072536766.unknown

_1072536572.unknown

_1072536521.unknown

_1072536543.unknown

_1072536314.unknown

_1072534563.unknown

_1072535713.unknown

_1072535805.unknown

_1072535921.unknown

_1072536098.unknown

_1072535835.unknown

_1072535786.unknown

_1072535796.unknown

_1072535723.unknown

_1072535583.unknown

_1072535623.unknown

_1072535635.unknown

_1072535606.unknown

_1072535568.unknown

_1072535575.unknown

_1072535201.unknown

_1072533753.unknown

_1072533801.unknown

_1072533818.unknown

_1072533829.unknown

_1072533812.unknown

_1072533777.unknown

_1072533794.unknown

_1072533763.unknown

_1072533595.unknown

_1072533684.unknown

_1072533696.unknown

_1072533612.unknown

_1072533516.unknown

_1072533545.unknown

_1072533505.unknown

