CHAPTER 7

DISLOCATIONS AND STRENGTHENING MECHANISMS

PROBLEM SOLUTIONS


Basic Concepts of Dislocations


Characteristics of Dislocations

7.1 To provide some perspective on the dimensions of atomic defects, consider a metal specimen that has a dislocation density of 104 mm-2.  Suppose that all the dislocations in 1000 mm3 (1 cm3) were somehow removed and linked end to end.  How far (in miles) would this chain extend?  Now suppose that the density is increased to 1010 mm-2 by cold working.  What would be the chain length of dislocations in 1000 mm3 of material?


Solution

The dislocation density is just the total dislocation length per unit volume of material (in this case per cubic millimeters).  Thus, the total length in 1000 mm3 of material having a density of 104 mm-2 is just


[image: image1.wmf]
Similarly, for a dislocation density of 1010 mm-2, the total length is


[image: image2.wmf]

7.2  Consider two edge dislocations of opposite sign and having slip planes that are separated by several atomic distances as indicated in the diagram. Briefly describe the defect that results when these two dislocations become aligned with each other.
[image: image3.png]





Solution

When the two edge dislocations become aligned, a planar region of vacancies will exist between the dislocations as:

[image: image4.png]Vacancies that extend
into and out of the
plane of the paper

—ooooo





7.3  Is it possible for two screw dislocations of opposite sign to annihilate each other? Explain your answer.


Solution

It is possible for two screw dislocations of opposite sign to annihilate one another if their dislocation lines are parallel.  This is demonstrated in the figure below.

[image: image5.png]LL L L L L L L L L L LY






7.4  For each of edge, screw, and mixed dislocations, cite the relationship between the direction of the applied shear stress and the direction of dislocation line motion.


Solution

For the various dislocation types, the relationships between the direction of the applied shear stress and the direction of dislocation line motion are as follows:


edge dislocation--parallel


screw dislocation--perpendicular


mixed dislocation--neither parallel nor perpendicular


Slip Systems

7.5  (a) Define a slip system.


(b) Do all metals have the same slip system? Why or why not?



Solution

(a)  A slip system is a crystallographic plane, and, within that plane, a direction along which dislocation motion (or slip) occurs.


(b)  All metals do not have the same slip system.  The reason for this is that for most metals, the slip system will consist of the most densely packed crystallographic plane, and within that plane the most closely packed direction.  This plane and direction will vary from crystal structure to crystal structure.


7.6  (a) Compare planar densities (Section 3.11 and Problem 3.54) for the (100), (110), and (111) planes for FCC.


(b) Compare planar densities (Problem 3.55) for the (100), (110), and (111) planes for BCC.


Solution

(a)  For the FCC crystal structure, the planar density for the (110) plane is given in Equation 3.11 as


[image: image6.wmf]

Furthermore, the planar densities of the (100) and (111) planes are calculated in Homework Problem 3.54, which are as follows:


[image: image7.wmf]

[image: image8.wmf]

(b)  For the BCC crystal structure, the planar densities of the (100) and (110) planes were determined in Homework Problem 3.55, which are as follows:


[image: image9.wmf]

[image: image10.wmf]

Below is a BCC unit cell, within which is shown a (111) plane.

[image: image11.png]



(a)

The centers of the three corner atoms, denoted by A, B, and C lie on this plane.  Furthermore, the (111) plane does not pass through the center of atom D, which is located at the unit cell center.  The atomic packing of this plane is presented in the following figure;  the corresponding atom positions from the Figure (a) are also noted.

[image: image12.png]/

R 1





(b)

Inasmuch as this plane does not pass through the center of atom D, it is not included in the atom count.  One sixth of each of the three atoms labeled A, B, and C is associated with this plane, which gives an equivalence of one-half atom.


In Figure (b) the triangle with A, B, and C at its corners is an equilateral triangle.  And, from Figure (b), the area of this triangle is 
[image: image13.wmf].  The triangle edge length, x, is equal to the length of a face diagonal, as indicated in Figure (a).  And its length is related to the unit cell edge length, a, as


[image: image14.wmf]
or


[image: image15.wmf]
For BCC,  
[image: image16.wmf] (Equation 3.3), and, therefore,


[image: image17.wmf]
Also, from Figure (b), with respect to the length y we may write


[image: image18.wmf]
which leads to 
[image: image19.wmf].  And, substitution for the above expression for x yields


[image: image20.wmf]
Thus, the area of this triangle is equal to


[image: image21.wmf]
And, finally, the planar density for this (111) plane is


[image: image22.wmf]

7.7  One slip system for the BCC crystal structure is 
[image: image23.wmf].  In a manner similar to Figure 7.6b, sketch a 
[image: image24.wmf]-type plane for the BCC structure, representing atom positions with circles. Now, using arrows, indicate two different 
[image: image25.wmf] slip directions within this plane.


Solution

Below is shown the atomic packing for a BCC 
[image: image26.wmf]-type plane.  The arrows indicate two different 
[image: image27.wmf]-type directions.

[image: image28.png]




7.8  One slip system for the HCP crystal structure is 
[image: image29.wmf]. In a manner similar to Figure 7.6b, sketch a 
[image: image30.wmf]-type plane for the HCP structure and, using arrows, indicate three different 
[image: image31.wmf] slip directions within this plane. You might find Figure 3.8 helpful.


Solution

Below is shown the atomic packing for an HCP 
[image: image32.wmf]-type plane.  The arrows indicate three different 
[image: image33.wmf]-type directions.
[image: image34.png]




7.9  Equations 7.1a and 7.1b, expressions for Burgers vectors for FCC and BCC crystal structures, are of the form

[image: image35.wmf]
where a is the unit cell edge length. Also, since the magnitudes of these Burgers vectors may be determined from the following equation:



[image: image36.wmf]
(7.10)
determine values of |b| for aluminum and chromium.  You may want to consult Table 3.1.



Solution

For Al, which has an FCC crystal structure, R = 0.1431 nm (Table 3.1) and a = 
[image: image37.wmf] = 0.4047 nm (Equation 3.1);  also, from Equation 7.1a, the Burgers vector for FCC metals is


[image: image38.wmf]
Therefore, the values for u, v, and w in Equation 7.10 are 1, 1, and 0, respectively.  Hence, the magnitude of the Burgers vector for Al is


[image: image39.wmf]

[image: image40.wmf]

For Cr which has a BCC crystal structure, R = 0.1249 nm (Table 3.1) and 
[image: image41.wmf] = 0.2884 nm (Equation 3.3);  also, from Equation 7.1b, the Burgers vector for BCC metals is


[image: image42.wmf]
Therefore, the values for u, v, and w in Equation 7.10 are 1, 1, and 1, respectively.  Hence, the magnitude of the Burgers vector for Cr is


[image: image43.wmf]

7.10  (a) In the manner of Equations 7.1a, 7.1b, and 7.1c, specify the Burgers vector for the simple cubic crystal structure. Its unit cell is shown in Figure 3.24. Also, simple cubic is the crystal structure for the edge dislocation of Figure 4.3, and for its motion as presented in Figure 7.1. You may also want to consult the answer to Concept Check 7.1.


(b) On the basis of Equation 7.10, formulate an expression for the magnitude of the Burgers vector, |b|, for simple cubic.



Solution

(a)  This part of the problem asks that we specify the Burgers vector for the simple cubic crystal structure (and suggests that we consult the answer to Concept Check 7.1).  This Concept Check asks that we select the slip system for simple cubic from four possibilities.  The correct answer is 
[image: image44.wmf].  Thus, the Burgers vector will lie in a 
[image: image45.wmf]-type direction.  Also, the unit slip distance is a (i.e., the unit cell edge length, Figures 4.3 and 7.1).  Therefore, the Burgers vector for simple cubic is


[image: image46.wmf]
Or, equivalently


[image: image47.wmf]

(b)  The magnitude of the Burgers vector, |b|, for simple cubic is


[image: image48.wmf]

Slip in Single Crystals

7.11  Sometimes cos ( cos ( in Equation 7.2 is termed the Schmid factor. Determine the magnitude of the Schmid factor for an FCC single crystal oriented with its [100] direction parallel to the loading axis.


Solution

We are asked to compute the Schmid factor for an FCC crystal oriented with its [100] direction parallel to the loading axis.  With this scheme, slip may occur on the (111) plane and in the 
[image: image49.wmf] direction as noted in the figure below.

[image: image50.png][111]





The angle between the [100] and 
[image: image51.wmf] directions, , may be determined using Equation 7.6


[image: image52.wmf]
where (for [100]) u1 = 1, v1 = 0, w1 = 0, and (for 
[image: image53.wmf]) u2 = 1, v2 = -1, w2 = 0.  Therefore,  is equal to

[image: image54.wmf]

[image: image55.wmf]
Now,  the angle  is equal to the angle between the normal to the (111) plane (which is the [111] direction), and the [100] direction.  Again from Equation 7.6, and for u1 = 1, v1 = 1, w1 = 1, and u2 = 1, v2 = 0, and w2 = 0, we have


[image: image56.wmf]

[image: image57.wmf]
Therefore, the Schmid factor is equal to


[image: image58.wmf]

7.12  Consider a metal single crystal oriented such that the normal to the slip plane and the slip direction are at angles of 43.1( and 47.9(, respectively, with the tensile axis.  If the critical resolved shear stress is 20.7 MPa (3000 psi), will an applied stress of 45 MPa (6500 psi) cause the single crystal to yield?  If not, what stress will be necessary?


Solution

This problem calls for us to determine whether or not a metal single crystal having a specific orientation and of given critical resolved shear stress will yield.  We are given that  = 43.1,  = 47.9, and that the values of the critical resolved shear stress and applied tensile stress are 20.7 MPa (3000 psi) and 45 MPa (6500 psi), respectively.  From Equation 7.2


[image: image59.wmf]
Since the resolved shear stress (22 MPa) is greater than the critical resolved shear stress (20.7 MPa), the single crystal will yield.


7.13  A single crystal of aluminum is oriented for a tensile test such that its slip plane normal makes an angle of 28.1( with the tensile axis.  Three possible slip directions make angles of 62.4(, 72.0(, and 81.1( with the same tensile axis.

(a) Which of these three slip directions is most favored?


(b) If plastic deformation begins at a tensile stress of 1.95 MPa (280 psi), determine the critical resolved shear stress for aluminum.


Solution

We are asked to compute the critical resolved shear stress for Al.  As stipulated in the problem,  = 28.1, while possible values for  are 62.4, 72.0, and 81.1.

(a)  Slip will occur along that direction for which (cos  cos ) is a maximum, or, in this case, for the largest cos .  Cosines for the possible  values are given below.
cos(62.4) = 0.46

cos(72.0) = 0.31

cos(81.1) = 0.15

Thus, the slip direction is at an angle of 62.4 with the tensile axis.


(b)  From Equation 7.4, the critical resolved shear stress is just


[image: image60.wmf]

[image: image61.wmf]

7.14  Consider a single crystal of silver oriented such that a tensile stress is applied along a [001] direction. If slip occurs on a (111) plane and in a 
[image: image62.wmf] direction, and is initiated at an applied tensile stress of 1.1 MPa (160 psi), compute the critical resolved shear stress.


Solution

This problem asks that we compute the critical resolved shear stress for silver.  In order to do this, we must employ Equation 7.4, but first it is necessary to solve for the angles  and  which are shown in the sketch below.

[image: image63.png]V4

[001] Direction w

1 Direction normal to
— (111) plane

(111) Plane
(slip plane)

y'd _
x N\ [101] Direction

(slip direction)





The angle  is the angle between the tensile axis—i.e., along the [001] direction—and the slip direction—i.e., 
[image: image64.wmf].  The angle  may be determined using Equation 7.6 as


[image: image65.wmf]
where (for [001]) u1 = 0, v1 = 0, w1 = 1, and (for 
[image: image66.wmf]) u2 = –1, v2 = 0, w2 = 1.  Therefore,  is equal to

[image: image67.wmf]

[image: image68.wmf]
Furthermore,  is the angle between the tensile axis—the [001] direction—and the normal to the slip plane—i.e., the (111) plane;  for this case this normal is along a [111] direction.  Therefore, again using Equation 7.6


[image: image69.wmf]

[image: image70.wmf]
And, finally, using Equation 7.4, the critical resolved shear stress is equal to


[image: image71.wmf]

[image: image72.wmf]

7.15  A single crystal of a metal that has the FCC crystal structure is oriented such that a tensile stress is applied parallel to the [110] direction. If the critical resolved shear stress for this material is 1.75 MPa, calculate the magnitude(s) of applied stress(es) necessary to cause slip to occur on the (111) plane in each of the 
[image: image73.wmf], 
[image: image74.wmf] and 
[image: image75.wmf] directions.


Solution

In order to solve this problem it is necessary to employ Equation 7.4, but first we need to solve for the  for  and  angles for the three slip systems.


For each of these three slip systems, the  will be the same—i.e., the angle between the direction of the applied stress, [110] and the normal to the (111) plane, that is, the [111] direction.  The angle  may be determined using Equation 7.6 as


[image: image76.wmf]
where (for [110]) u1 = 1, v1 = 1, w1 = 0, and (for [111]) u2 = 1, v2 = 1, w2 = 1.  Therefore,  is equal to

[image: image77.wmf]

[image: image78.wmf]
Let us now determine  for the 
[image: image79.wmf] slip direction.  Again, using Equation 7.6 where u1 = 1, v1 = 1, w1 = 0 (for [110]), and u2 = 1, v2 = –1, w2 = 0 (for 
[image: image80.wmf].  Therefore,  is determined as

[image: image81.wmf]

[image: image82.wmf]
Now, we solve for the yield strength for this (111)–
[image: image83.wmf] slip system using Equation 7.4 as


[image: image84.wmf]

[image: image85.wmf]
which means that slip will not occur on this (111)–
[image: image86.wmf] slip system.


Now, we must determine the value of  for the (111)–
[image: image87.wmf] slip system—that is, the angle between the [110] and 
[image: image88.wmf] directions.  Again using Equation 7.6


[image: image89.wmf]

[image: image90.wmf]
Now, we solve for the yield strength for this (111)–
[image: image91.wmf] slip system using Equation 7.4 as


[image: image92.wmf]

[image: image93.wmf]

And, finally, for the (111)–
[image: image94.wmf] slip system,  is computed using Equation 7.6 as follows:

[image: image95.wmf]

[image: image96.wmf]
Thus, since the values of  and for this (110)–
[image: image97.wmf] slip system are the same as for (111)–
[image: image98.wmf], so also will y be the same—viz 4.29 MPa.


7.16  (a) A single crystal of a metal that has the BCC crystal structure is oriented such that a tensile stress is applied in the [010] direction. If the magnitude of this stress is 2.75 MPa, compute the resolved shear stress in the 
[image: image99.wmf] direction on each of the (110) and (101) planes.


(b) On the basis of these resolved shear stress values, which slip system(s) is (are) most favorably oriented?



Solution

(a)  This part of the problem asks, for a BCC metal, that we compute the resolved shear stress in the 
[image: image100.wmf] direction on each of the (110) and (101) planes.  In order to solve this problem it is necessary to employ Equation 7.2, which means that we first need to solve for the  for angles  and  for the three slip systems.


For each of these three slip systems, the  will be the same—i.e., the angle between the direction of the applied stress, [010] and the slip direction, 
[image: image101.wmf].  This angle  may be determined using Equation 7.6


[image: image102.wmf]
where (for [010]) u1 = 0, v1 = 1, w1 = 0, and (for 
[image: image103.wmf]) u2 = –1, v2 = 1, w2 = 1.  Therefore,  is determined as

[image: image104.wmf]

[image: image105.wmf]
Let us now determine  for the angle between the direction of the applied tensile stress—i.e., the [010] direction—and the normal to the (110) slip plane—i.e., the [110] direction.  Again, using Equation 7.6 where u1 = 0, v1 = 1, w1 = 0 (for [010]), and u2 = 1, v2 = 1, w2 = 0 (for [110]),  is equal to

[image: image106.wmf]

[image: image107.wmf]
Now, using Equation 7.2


[image: image108.wmf]
we solve for the resolved shear stress for this slip system as


[image: image109.wmf]

Now, we must determine the value of  for the (101)–
[image: image110.wmf] slip system—that is, the angle between the direction of the applied stress, [010], and the normal to the (101) plane—i.e., the [101] direction.  Again using Equation 7.6


[image: image111.wmf]

[image: image112.wmf]
Thus, the resolved shear stress for this (101)–
[image: image113.wmf] slip system is


[image: image114.wmf]

(b)  The most favored slip system(s) is (are) the one(s) that has (have) the largest R value.  Therefore, the (110)–
[image: image115.wmf] is the most favored since its R (1.12 MPa) is greater than the R value for 
[image: image116.wmf] (viz., 0 MPa).

7.17  Consider a single crystal of some hypothetical metal that has the FCC crystal structure and is oriented such that a tensile stress is applied along a 
[image: image117.wmf] direction. If slip occurs on a (111) plane and in a 
[image: image118.wmf] direction, compute the stress at which the crystal yields if its critical resolved shear stress is 3.42 MPa.


Solution

This problem asks for us to determine the tensile stress at which a FCC metal yields when the stress is applied along a 
[image: image119.wmf] direction such that slip occurs on a (111) plane and in a 
[image: image120.wmf] direction;  the critical resolved shear stress for this metal is 3.42 MPa.  To solve this problem we use Equation 7.4;  however it is first necessary to determine the values of  and .  These determinations are possible using Equation 7.6.   Now,  is the angle between 
[image: image121.wmf] and 
[image: image122.wmf] directions.  Therefore, relative to Equation 7.6 let us take u1 = –1, v1 = 0, and w1 = 2, as well as u2 = –1, v2 = 0, and w2 = 1.  This leads to


[image: image123.wmf]

[image: image124.wmf]

[image: image125.wmf]
Now for the determination of , the normal to the (111) slip plane is the [111] direction.  Again using Equation 7.6, where we now take u1 = –1, v1 = 0, w1 = 2 (for 
[image: image126.wmf]), and u2 = 1, v2 = 1, w2 = 1 (for [111]).  Thus,


[image: image127.wmf]

[image: image128.wmf]
It is now possible to compute the yield stress (using Equation 7.4) as


[image: image129.wmf]

7.18  The critical resolved shear stress for iron is 27 MPa (4000 psi).  Determine the maximum possible yield strength for a single crystal of Fe pulled in tension.


Solution

In order to determine the maximum possible yield strength for a single crystal of Fe pulled in tension, we simply employ Equation 7.5 as


[image: image130.wmf]

Deformation by Twinning

7.19  List four major differences between deformation by twinning and deformation by slip relative to mechanism, conditions of occurrence, and final result.


Solution

Four major differences between deformation by twinning and deformation by slip are as follows:  (1) with slip deformation there is no crystallographic reorientation, whereas with twinning there is a reorientation;  (2) for slip, the atomic displacements occur in atomic spacing multiples, whereas for twinning, these displacements may be other than by atomic spacing multiples;  (3) slip occurs in metals having many slip systems, whereas twinning occurs in metals having relatively few slip systems;  and (4) normally slip results in relatively large deformations, whereas only small deformations result for twinning.


Strengthening by Grain Size Reduction

7.20  Briefly explain why small-angle grain boundaries are not as effective in interfering with the slip process as are high-angle grain boundaries.


Solution

Small-angle grain boundaries are not as effective in interfering with the slip process as are high-angle grain boundaries because there is not as much crystallographic misalignment in the grain boundary region for small-angle, and therefore not as much change in slip direction.


7.21  Briefly explain why HCP metals are typically more brittle than FCC and BCC metals.


Solution

Hexagonal close packed metals are typically more brittle than FCC and BCC metals because there are fewer slip systems in HCP.


7.22  Describe in your own words the three strengthening mechanisms discussed in this chapter (i.e., grain size reduction, solid-solution strengthening, and strain hardening). Be sure to explain how dislocations are involved in each of the strengthening techniques.

These three strengthening mechanisms are described in Sections 7.8, 7.9, and 7.10.


7.23  (a) From the plot of yield strength versus (grain diameter)–1/2 for a 70 Cu–30 Zn cartridge brass, Figure 7.15, determine values for the constants σ0 and ky in Equation 7.7.


(b) Now predict the yield strength of this alloy when the average grain diameter is 1.0 ( 10-3 mm.


Solution

(a)  Perhaps the easiest way to solve for 0 and ky in Equation 7.7 is to pick two values each of y and d-1/2 from Figure 7.15, and then solve two simultaneous equations, which may be created.  For example


d-1/2 (mm) -1/2
y (MPa)


4
75


12
175

The two equations are thus


[image: image131.wmf]

[image: image132.wmf]
Solution of these equations yield the values of


[image: image133.wmf]
0 = 25 MPa  (3630 psi)


(b)  When d = 1.0 ( 10-3 mm, d-1/2 = 31.6 mm-1/2, and, using Equation 7.7,


[image: image134.wmf]

[image: image135.wmf]

7.24  The lower yield point for an iron that has an average grain diameter of 5 ( 10-2 mm is 135 MPa (19,500 psi).  At a grain diameter of 8 ( 10-3 mm, the yield point increases to 260 MPa (37,500 psi).  At what grain diameter will the lower yield point be 205 MPa (30,000 psi)?


Solution

The best way to solve this problem is to first establish two simultaneous expressions of Equation 7.7, solve for 0 and ky, and finally determine the value of d when y = 205 MPa.  The data pertaining to this problem may be tabulated as follows:


y
d (mm)
d-1/2 (mm)-1/2

135 MPa
5 ( 10-2
4.47


260 MPa
8 ( 10-3
11.18

The two equations thus become


[image: image136.wmf]

[image: image137.wmf]
Which yield the values, 0 = 51.7 MPa and ky = 18.63 MPa(mm)1/2.  At a yield strength of 205 MPa


[image: image138.wmf]
or d-1/2 = 8.23 (mm) -1/2, which gives d = 1.48 ( 10-2 mm.


7.25  If it is assumed that the plot in Figure 7.15 is for noncold-worked brass, determine the grain size of the alloy in Figure 7.19;  assume its composition is the same as the alloy in Figure 7.15.


Solution

This problem asks that we determine the grain size of the brass for which is the subject of Figure 7.19.  From Figure 7.19a, the yield strength of brass at 0%CW is approximately 175 MPa (26,000 psi).  This yield strength from Figure 7.15 corresponds to a d-1/2 value of approximately 12.0 (mm) -1/2. Thus, d = 6.9 ( 10-3 mm.


Solid-Solution Strengthening

7.26  In the manner of Figures 7.17b and 7.18b, indicate the location in the vicinity of an edge dislocation at which an interstitial impurity atom would be expected to be situated. Now briefly explain in terms of lattice strains why it would be situated at this position.


Solution

Below is shown an edge dislocation and where an interstitial impurity atom would be located.  Compressive lattice strains are introduced by the impurity atom.  There will be a net reduction in lattice strain energy when  these lattice strains partially cancel tensile strains associated with the edge dislocation;  such tensile strains exist just below the bottom of the extra half-plane of atoms (Figure 7.4).

[image: image139.png]Atom

Interstitial Impurity

OOVO00O

OO
ole! OO
00000

OO0000





Strain Hardening

7.27  (a) Show, for a tensile test, that

[image: image140.wmf]
if there is no change in specimen volume during the deformation process (i.e., A0l0 = Adld).


(b) Using the result of part (a), compute the percent cold work experienced by naval brass (the stress-strain behavior of which is shown in Figure 6.12) when a stress of 400 MPa (58,000 psi) is applied.


Solution

(a)  From Equation 7.8


[image: image141.wmf]
Which is also equal to


[image: image142.wmf]
since Ad/A0 = l0/ld, the conservation of volume stipulation given in the problem statement.  Now, from the definition of engineering strain (Equation 6.2)


[image: image143.wmf]
Or,


[image: image144.wmf]
Substitution for l0/ ld into the %CW expression above gives


[image: image145.wmf]

(b)  From Figure 6.12, a stress of 400 MPa (58,000 psi) corresponds to a strain of 0.13.  Using the above expression


[image: image146.wmf]

7.28  Two previously undeformed cylindrical specimens of an alloy are to be strain hardened by reducing their cross-sectional areas (while maintaining their circular cross sections).  For one specimen, the initial and deformed radii are 16 mm and 11 mm, respectively.  The second specimen, with an initial radius of 12 mm, must have the same deformed hardness as the first specimen;  compute the second specimen's radius after deformation.


Solution

In order for these two cylindrical specimens to have the same deformed hardness, they must be deformed to the same percent cold work.  For the first specimen


[image: image147.wmf]

[image: image148.wmf]
For the second specimen, the deformed radius is computed using the above equation and solving for rd as


[image: image149.wmf]

[image: image150.wmf]

7.29  Two previously undeformed specimens of the same metal are to be plastically deformed by reducing their cross-sectional areas.  One has a circular cross section, and the other is rectangular; during deformation the circular cross section is to remain circular, and the rectangular is to remain as such.  Their original and deformed dimensions are as follows:

	
	Circular (diameter, mm)
	Rectangular (mm)

	Original dimensions
	15.2
	125 × 175

	Deformed dimensions
	11.4
	75 × 200



Which of these specimens will be the hardest after plastic deformation, and why?


Solution

The hardest specimen will be the one that has experienced the greatest degree of cold work.  Therefore, all we need do is to compute the %CW for each specimen using Equation 7.8.  For the circular one


[image: image151.wmf]

[image: image152.wmf]

[image: image153.wmf]
For the rectangular one


[image: image154.wmf]
Therefore, the deformed circular specimen will be harder.


7.30  A cylindrical specimen of cold-worked copper has a ductility (%EL) of 25%.  If its cold-worked radius is 10 mm (0.40 in.), what was its radius before deformation?


Solution

This problem calls for us to calculate the precold-worked radius of a cylindrical specimen of copper that has a cold-worked ductility of 25%EL.  From Figure 7.19c, copper that has a ductility of 25%EL will have experienced a deformation of about 11%CW.  For a cylindrical specimen, Equation 7.8 becomes


[image: image155.wmf]
Since rd = 10 mm (0.40 in.), solving for r0 yields


[image: image156.wmf]

7.31  (a) What is the approximate ductility (%EL) of a brass that has a yield strength of 275 MPa (40,000 psi)?


(b) What is the approximate Brinell hardness of a 1040 steel having a yield strength of 690 MPa (100,000 psi)?


Solution

(a) In order to solve this problem, it is necessary to consult Figures 7.19a and 7.19c.  From Figure 7.19a, a yield strength of 275 MPa for brass corresponds to 10%CW.  A brass that has been cold-worked 10% will have a ductility of about 43%EL [Figure 7.19c].


(b)  This portion of the problem asks for the Brinell hardness of a 1040 steel having a yield strength of 690 MPa (100,000 psi).  From Figure 7.19a, a yield strength of 690 MPa for a 1040 steel corresponds to about 10%CW.  A 1040 steel that has been cold worked 10% will have a tensile strength of about 780 MPa [Figure 7.19b].  Finally, using Equation 6.20a


[image: image157.wmf]

7.32  Experimentally, it has been observed for single crystals of a number of metals that the critical resolved shear stress τcrss is a function of the dislocation density ρD as

[image: image158.wmf]
where τ0 and A are constants. For copper, the critical resolved shear stress is 2.10 MPa (305 psi) at a dislocation density of 105 mm-2.  If it is known that the value of A for copper is 6.35 ( 10-3 MPa-mm (0.92 psi-mm), compute the tcrss at a dislocation density of 107 mm-2.


Solution

We are asked in this problem to compute the critical resolved shear stress at a dislocation density of 107 mm-2.  It is first necessary to compute the value of the constant 0 (in the equation provided in the problem statement) from the one set of data as


[image: image159.wmf]

[image: image160.wmf]
Now, the critical resolved shear stress may be determined at a dislocation density of 107 mm-2 as


[image: image161.wmf]

[image: image162.wmf]

Recovery


Recrystallization


Grain Growth

7.33  Briefly cite the differences between recovery and recrystallization processes.


Solution

For recovery, there is some relief of internal strain energy by dislocation motion;  however, there are virtually no changes in either the grain structure or mechanical characteristics.  During recrystallization, on the other hand, a new set of strain-free grains forms, and the material becomes softer and more ductile.


7.34  Estimate the fraction of recrystallization from the photomicrograph in Figure 7.21c.


Solution

Below is shown a square grid onto which is superimposed the recrystallized regions from the micrograph. Approximately 400 squares lie within the recrystallized areas, and since there are 672 total squares, the specimen is about 60% recrystallized.

[image: image163.png]L1

Ll

11






7.35  Explain the differences in grain structure for a metal that has been cold worked and one that has been cold worked and then recrystallized.


Solution

During cold-working, the grain structure of the metal has been distorted to accommodate the deformation.  Recrystallization produces grains that are equiaxed and smaller than the parent grains.


7.36  (a) What is the driving force for recrystallization?


(b) For grain growth?


Solution

(a)  The driving force for recrystallization is the difference in internal energy between the strained and unstrained material.


(b)  The driving force for grain growth is the reduction in grain boundary energy as the total grain boundary area decreases.


7.37  (a) From Figure 7.25, compute the length of time required for the average grain diameter to increase from 0.01 to 0.1 mm at 500(C for this brass material.


(b) Repeat the calculation at 600°C.



Solution

(a)  At 500C, the time necessary for the average grain diameter to grow to increase from 0.01 to 0.1 mm is approximately 3500 min.


(b)  At 600C the time required for this same grain size increase is approximately 150 min.


7.38  The average grain diameter for a brass material was measured as a function of time at 650°C, which is tabulated below at two different times:

	Time (min)
	Grain Diameter (mm)

	30
	3.9 × 10–2

	90
	6.6 × 10–2



(a) What was the original grain diameter?


(b) What grain diameter would you predict after 150 min at 650°C?



Solution

(a)  Using the data given and Equation 7.9 (taking n = 2), we may set up two simultaneous equations with d0 and K as unknowns;  thus


[image: image164.wmf]

[image: image165.wmf]
Solution of these expressions yields a value for d0, the original grain diameter, of

d0 = 0.01 mm,

and a value for K of 4.73 ( 10-5 mm2/min


(b)  At 150 min, the diameter d is computed using a rearranged form of Equation 7.9 as


[image: image166.wmf]

[image: image167.wmf]

7.39  An undeformed specimen of some alloy has an average grain diameter of 0.040 mm.  You are asked to reduce its average grain diameter to 0.010 mm.  Is this possible?  If so, explain the procedures you would use and name the processes involved.  If it is not possible, explain why.


Solution

Yes, it is possible to reduce the average grain diameter of an undeformed alloy specimen from 0.040 mm to 0.010 mm.  In order to do this, plastically deform the material at room temperature (i.e., cold work it), and then anneal at an elevated temperature in order to allow recrystallization and some grain growth to occur until the average grain diameter is 0.010 mm.


7.40  Grain growth is strongly dependent on temperature (i.e., rate of grain growth increases with increasing temperature), yet temperature is not explicitly given as a part of Equation 7.9.


(a)  Into which of the parameters in this expression would you expect temperature to be included?


(b)  On the basis of your intuition, cite an explicit expression for this temperature dependence.


Solution

(a)  The temperature dependence of grain growth is incorporated into the constant K in Equation 7.9.


(b)  The explicit expression for this temperature dependence is of the form


[image: image168.wmf]
in which K0 is a temperature-independent constant, the parameter Q is an activation energy, and R and T are the gas constant and absolute temperature, respectively.


7.41 An uncold-worked brass specimen of average grain size 0.008 mm has a yield strength of 160 MPa (23,500 psi).  Estimate the yield strength of this alloy after it has been heated to 600(C for 1000 s, if it is known that the value of ky is 12.0 MPa-mm1/2 (1740 psi-mm1/2).


Solution

In order to solve this problem, it is first necessary to calculate the constant 0 in Equation 7.7 as


[image: image169.wmf]

[image: image170.wmf]
Next, we must determine the average grain size after the heat treatment.  From Figure 7.25 at 600C after 1000 s (16.7 min) the average grain size of a brass material is about 0.20 mm.  Therefore, calculating y at this new grain size using Equation 7.7 we get


[image: image171.wmf]

[image: image172.wmf]
DESIGN PROBLEMS


Strain Hardening


Recrystallization

7.D1  Determine whether or not it is possible to cold work steel so as to give a minimum Brinell hardness of 225, and at the same time have a ductility of at least 12%EL.  Justify your decision.


Solution

The tensile strength corresponding to a Brinell hardness of 225 may be determined using Equation 6.20a as


[image: image173.wmf]
Furthermore, from Figure 7.19b, in order to achieve a tensile strength of 776 MPa, deformation of at least 9%CW is necessary.  Finally, if we cold work the steel to 9%CW, then the ductility is 17%EL from Figure 7.19c.  Therefore, it is possible to meet both of these criteria by plastically deforming the steel.


7.D2  Determine whether or not it is possible to cold work brass so as to give a minimum Brinell hardness of 120 and at the same time have a ductility of at least 20%EL.  Justify your decision.


Solution

According to Figure 6.19, a Brinell hardness of 120 corresponds to a tensile strength of 440 MPa (63,500 psi.)  Furthermore, from Figure 7.19b, in order to achieve a tensile strength of 440 MPa, deformation of at least 26%CW is necessary.  Finally, if we are to achieve a ductility of at least 20%EL, then a maximum deformation of 23%CW is possible from Figure 7.19c.  Therefore, it is not possible to meet both of these criteria by plastically deforming brass.


7.D3  A cylindrical specimen of cold-worked steel has a Brinell hardness of 250.

(a) Estimate its ductility in percent elongation.


(b) If the specimen remained cylindrical during deformation and its original radius was 5 mm (0.20 in.), determine its radius after deformation.


Solution

(a)  From Figure 6.19, a Brinell hardness of 250 corresponds to a tensile strength of 860 MPa (125,000 psi), which, from Figure 7.19b, requires a deformation of 25%CW.  Furthermore, 25%CW yields a ductility of about 11%EL for steel, Figure 7.19c.


(b)  We are now asked to determine the radius after deformation if the uncold-worked radius is 5 mm (0.20 in.).  From Equation 7.8 and for a cylindrical specimen


[image: image174.wmf]
Now, solving for rd from this expression, we get


[image: image175.wmf]

[image: image176.wmf]

7.D4  It is necessary to select a metal alloy for an application that requires a yield strength of at least 345 MPa (50,000 psi) while maintaining a minimum ductility (%EL) of 20%. If the metal may be cold worked, decide which of the following are candidates:  copper, brass, and a 1040 steel.  Why?


Solution

For each of these alloys, the minimum cold work necessary to achieve the yield strength may be determined from Figure 7.19a, while the maximum possible cold work for the ductility is found in Figure 7.19c.  These data are tabulated below.



Yield Strength
Ductility



(> 345 MPa)
(> 20%EL)

Steel
Any %CW
< 5%CW


Brass
> 20%CW
< 23%CW


Copper
> 54%CW
< 15%CW

Thus, both the 1040 steel and brass are possible candidates since for these alloys there is an overlap of percents coldwork to give the required minimum yield strength and ductility values.


7.D5  A cylindrical rod of 1040 steel originally 15.2 mm (0.60 in.) in diameter is to be cold worked by drawing;  the circular cross section will be maintained during deformation.  A cold-worked tensile strength in excess of 840 MPa (122,000 psi) and a ductility of at least 12%EL are desired.  Furthermore, the final diameter must be 10 mm (0.40 in.).  Explain how this may be accomplished.


Solution

First let us calculate the percent cold work and attendant tensile strength and ductility if the drawing is carried out without interruption.  From Equation 7.8


[image: image177.wmf]

[image: image178.wmf]
At 56%CW, the steel will have a tensile strength on the order of 920 MPa (133,000 psi) [Figure 7.19b], which is adequate;  however, the ductility will be less than 10%EL [Figure 7.19c], which is insufficient.


Instead of performing the drawing in a single operation, let us initially draw some fraction of the total deformation, then anneal to recrystallize, and, finally, cold-work the material a second time in order to achieve the final diameter, tensile strength, and ductility.


Reference to Figure 7.19b indicates that 20%CW is necessary to yield a tensile strength of 840 MPa (122,000 psi).  Similarly, a maximum of 21%CW is possible for 12%EL [Figure 7.19c].  The average of these extremes is 20.5%CW.  Again using Equation 7.8, if the final diameter after the first drawing is 
[image: image179.wmf], then

[image: image180.wmf]
And, solving the above expression for 
[image: image181.wmf], yields 


[image: image182.wmf]

7.D6  A cylindrical rod of copper originally 16.0 mm (0.625 in.) in diameter is to be cold worked by drawing; the circular cross section will be maintained during deformation.  A cold-worked yield strength in excess of 250 MPa (36,250 psi) and a ductility of at least 12%EL are desired. Furthermore, the final diameter must be 11.3 mm (0.445 in.).  Explain how this may be accomplished.


Solution

Let us first calculate the percent cold work and attendant yield strength and ductility if the drawing is carried out without interruption.  From Equation 7.8


[image: image183.wmf]

[image: image184.wmf]
At 50%CW, the copper will have a yield strength on the order of 330 MPa (48,000 psi), Figure 7.19a, which is adequate;  however, the ductility will be about 4%EL, Figure 7.19c, which is insufficient.


Instead of performing the drawing in a single operation, let us initially draw some fraction of the total deformation, then anneal to recrystallize, and, finally, cold work the material a second time in order to achieve the final diameter, yield strength, and ductility.


Reference to Figure 7.19a indicates that 21%CW is necessary to give a yield strength of 250 MPa.  Similarly, a maximum of 23%CW is possible for 12%EL [Figure 7.19c].  The average of these two values is 22%CW, which we will use in the calculations. Thus, to achieve both the specified yield strength and ductility, the copper must be deformed to 22%CW.  If the final diameter after the first drawing is 
[image: image185.wmf], then, using Equation 7.8


[image: image186.wmf]
And, solving for 
[image: image187.wmf] from the above expression yields


[image: image188.wmf]

7.D7  A cylindrical 1040 steel rod having a minimum tensile strength of 865 MPa (125,000 psi), a ductility of at least 10%EL, and a final diameter of 6.0 mm (0.25 in.) is desired.  Some 7.94 mm (0.313 in.) diameter 1040 steel stock, which has been cold worked 20% is available.  Describe the procedure you would follow to obtain this material.  Assume that 1040 steel experiences cracking at 40%CW.


Solution

This problem calls for us to cold work some 1040 steel stock that has been previously cold worked in order to achieve minimum tensile strength and ductility values of 865 MPa (125,000 psi) and 10%EL, respectively, while the final diameter must be 6.0 mm (0.25 in.).  Furthermore, the material may not be deformed beyond 40%CW.  Let us start by deciding what percent coldwork is necessary for the minimum tensile strength and ductility values, assuming that a recrystallization heat treatment is possible.  From Figure 7.19b, at least 25%CW is required for a tensile strength of 865 MPa.  Furthermore, according to Figure 7.19c, 10%EL corresponds a maximum of 30%CW.  Let us take the average of these two values (i.e., 27.5%CW), and determine what previous specimen diameter is required to yield a final diameter of 6.0 mm.  For cylindrical specimens, Equation 7.8 takes the form


[image: image189.wmf]
Solving for the original diameter d0 yields


[image: image190.wmf]

Now, let us determine its undeformed diameter realizing that a diameter of 7.94 mm corresponds to 20%CW.  Again solving for d0 using the above equation and assuming dd = 7.94 mm yields


[image: image191.wmf]
At this point let us see if it is possible to deform the material from 8.88 mm to 7.05 mm without exceeding the 40%CW limit.  Again employing Equation 7.8


[image: image192.wmf]

In summary, the procedure which can be used to produce the desired material would be as follows:  cold work the as-received stock to 7.05 mm (0.278 in.), heat treat it to achieve complete recrystallization, and then cold work the material again to 6.0 mm (0.25 in.), which will give the desired tensile strength and ductility.

PAGE  
Excerpts from this work may be reproduced by instructors for distribution on a not-for-profit basis for testing or instructional purposes only to students enrolled in courses for which the textbook has been adopted.  Any other reproduction or translation of this work beyond that permitted by Sections 107 or 108 of the 1976 United States Copyright Act without the permission of the copyright owner is unlawful.

_1175863771.unknown

_1175930138.unknown

_1179306956.unknown

_1179310749.unknown

_1179311270.unknown

_1179312123.unknown

_1179313849.unknown

_1179317868.unknown

_1198567264.unknown

_1179318024.unknown

_1179316915.unknown

_1179312719.unknown

_1179313738.unknown

_1179312139.unknown

_1179311967.unknown

_1179312008.unknown

_1179311586.unknown

_1179311090.unknown

_1179311153.unknown

_1179310812.unknown

_1179310508.unknown

_1179310643.unknown

_1179310731.unknown

_1179310532.unknown

_1179307855.unknown

_1179310460.unknown

_1179307685.unknown

_1175931644.unknown

_1175938452.unknown

_1175940334.unknown

_1176021116.unknown

_1176021176.unknown

_1176021532.unknown

_1176021567.unknown

_1176021193.unknown

_1176021139.unknown

_1176020801.unknown

_1176020826.unknown

_1175940392.unknown

_1175939924.unknown

_1175939966.unknown

_1175939459.unknown

_1175933126.unknown

_1175937538.unknown

_1175937832.unknown

_1175937460.unknown

_1175932208.unknown

_1175932297.unknown

_1175931942.unknown

_1175930620.unknown

_1175931047.unknown

_1175931164.unknown

_1175930717.unknown

_1175930585.unknown

_1175930598.unknown

_1175930240.unknown

_1175886473.unknown

_1175928611.unknown

_1175929095.unknown

_1175929624.unknown

_1175930110.unknown

_1175929178.unknown

_1175928746.unknown

_1175929069.unknown

_1175928712.unknown

_1175887489.unknown

_1175887866.unknown

_1175928584.unknown

_1175887508.unknown

_1175886516.unknown

_1175887146.unknown

_1175886491.unknown

_1175884756.unknown

_1175885129.unknown

_1175885890.unknown

_1175886069.unknown

_1175885492.unknown

_1175885037.unknown

_1175885086.unknown

_1175884892.unknown

_1175882457.unknown

_1175882895.unknown

_1175884698.unknown

_1175882677.unknown

_1175881682.unknown

_1175882265.unknown

_1175881554.unknown

_1073546474.unknown

_1158320003.unknown

_1175863309.unknown

_1175863582.unknown

_1175863669.unknown

_1175863754.unknown

_1175863645.unknown

_1175863458.unknown

_1175863494.unknown

_1175863346.unknown

_1158321534.unknown

_1158322584.unknown

_1158322952.unknown

_1175862237.unknown

_1175863282.unknown

_1158323053.unknown

_1158323093.unknown

_1158322805.unknown

_1158322913.unknown

_1158322606.unknown

_1158322468.unknown

_1158322509.unknown

_1158321653.unknown

_1158321180.unknown

_1158321337.unknown

_1158321429.unknown

_1158321216.unknown

_1158320246.unknown

_1158320936.unknown

_1158320177.unknown

_1158313389.unknown

_1158315448.unknown

_1158319937.unknown

_1158319969.unknown

_1158319869.unknown

_1158313518.unknown

_1158315421.unknown

_1158313448.unknown

_1073546774.unknown

_1158312114.unknown

_1158313078.unknown

_1158313102.unknown

_1158313170.unknown

_1158312423.unknown

_1158311458.unknown

_1073550900.unknown

_1073546671.unknown

_1073546745.unknown

_1073546615.unknown

_1072631914.unknown

_1072635596.unknown

_1072636645.unknown

_1072638702.unknown

_1072641022.unknown

_1073546185.unknown

_1073546371.unknown

_1072641518.unknown

_1072642048.unknown

_1072639770.unknown

_1072640865.unknown

_1072638836.unknown

_1072637188.unknown

_1072638697.unknown

_1072637146.unknown

_1072636143.unknown

_1072636194.unknown

_1072636201.unknown

_1072636171.unknown

_1072636101.unknown

_1072636119.unknown

_1072635988.unknown

_1072635501.unknown

_1072635534.unknown

_1072635560.unknown

_1072635514.unknown

_1072633216.unknown

_1072635386.unknown

_1072631948.unknown

_1072630813.unknown

_1072630850.unknown

_1072630870.unknown

_1072630877.unknown

_1072630859.unknown

_1072630831.unknown

_1072630843.unknown

_1072630819.unknown

_1072630374.unknown

_1072630791.unknown

_1072630803.unknown

_1072630380.unknown

_1072630331.unknown

_1072630340.unknown

_1072630153.unknown

