ENGR 244 Mechanics of Materials

## Section AP-X

# EXPERIMENT No. 2: Tension Test on Metals

Yuen Shan Chan

27749104

Monday June 15th 2015

## Analysis of results

- Sample calculation for stress for aluminum (*):
σ=PA=508 N12.19 mm2=41.666 MPa

| Aluminum |  |  |  |
| --- | --- | --- | --- |
| Load (N) | Deformation (mm) | Stress (Mpa) | Strain |
| 508 | 0 | 41.66595949* | 0 |
| 1001 | 0.07 | 82.1016249 | 0.0007 |
| 1502 | 0.15 | 123.1934472 | 0.0015 |
| 2006 | 0.22 | 164.5313282 | 0.0022 |
| 2507 | 0.3 | 205.6231505 | 0.003 |
| 3005 | 0.39 | 246.4689139 | 0.0039 |
| 3200 | 0.62 | 262.4627369 | 0.0062 |
| 3400 | 1.99 | 278.866658 | 0.0199* |
| 3560 | 4.38 | 291.9897948 | 0.0438 |
| 3605 | 4.88 | 295.6806771 | 0.0488 |
| 3655 | 5.38 | 299.7816573 | 0.0538 |
| 3629 | 5.88 | 297.6491476 | 0.0588 |
| 3657 | 6.38 | 299.9456966 | 0.0638 |
| 3704 | 6.88 | 303.800618 | 0.0688 |
| 3713 | 7.38 | 304.5387945 | 0.0738 |
| 3623 | 7.88 | 297.15703 | 0.0788 |
| 3224 | 8.44 | 264.4312075 | 0.0844 |

Sample calculation for strain for aluminum (*): 
ε=δL=1.99 mm100 mm=0.0199

| Steel |  |  |  |
| --- | --- | --- | --- |
| Load (N) | Deformation (mm) | Stress (MPa) | Strain |
| 500 | 0 | 40.18962731 | 0 |
| 1016 | 0.01 | 81.66532268 | 0.0001 |
| 1519 | 0.02 | 122.0960878 | 0.0002 |
| 2003 | 0.03 | 160.999647 | 0.0003 |
| 2506 | 0.05 | 201.4304121 | 0.0005 |
| 3004 | 0.07 | 241.4592809 | 0.0007 |
| 3515 | 0.08 | 282.53308 | 0.0008 |
| 4002 | 0.1 | 321.677777 | 0.001 |
| 4512 | 0.12 | 362.6711968 | 0.0012 |
| 5007 | 0.14 | 402.4589278 | 0.0014 |
| 5204 | 0.16 | 418.293641 | 0.0016 |
| 5403 | 0.17 | 434.2891127 | 0.0017 |
| 5605 | 0.18 | 450.5257221 | 0.0018 |
| 5805 | 0.21 | 466.601573 | 0.0021 |
| 6012 | 0.24 | 483.2400787 | 0.0024 |
| 6207 | 0.29 | 498.9140334 | 0.0029 |
| 6400 | 0.33 | 514.4272295 | 0.0033 |
| 6607 | 0.44 | 531.0657352 | 0.0044 |
| 6805 | 0.54 | 546.9808276 | 0.0054 |
| 7012 | 0.72 | 563.6193333 | 0.0072 |
| 7230 | 0.85 | 581.1420108 | 0.0085 |
| 7264 | 1.07 | 583.8749055 | 0.0107 |
| 7371 | 1.32 | 592.4754857 | 0.0132 |
| 7431 | 1.57 | 597.298241 | 0.0157 |
| 7427 | 1.82 | 596.976724 | 0.0182 |
| 7539 | 2.07 | 605.9792005 | 0.0207 |
| 7579 | 2.32 | 609.1943707 | 0.0232 |
| 7515 | 2.57 | 604.0500984 | 0.0257 |
| 7612 | 2.82 | 611.8468861 | 0.0282 |
| 7615 | 3.07 | 612.0880239 | 0.0307 |
| 7617 | 3.33 | 612.2487824 | 0.0333 |
| 7603 | 3.58 | 611.1234728 | 0.0358 |
| 7518 | 3.82 | 604.2912362 | 0.0382 |
| 7449 | 4.07 | 598.7450676 | 0.0407 |
| 7179 | 4.42 | 577.0426689 | 0.0442 |
| 7044 | 4.67 | 566.1914695 | 0.0467 |
| 6803 | 4.92 | 546.8200691 | 0.0492 |
| 6303 | 5.27 | 506.6304418 | 0.0527 |
| 5804 | 5.52 | 466.5211938 | 0.0552 |
| 5325 | 5.77 | 428.0195308 | 0.0577 |

  - Aluminum yield strength = 273.89 MPa

Steel yield strength =495.72 MPa

  - Ultimate strength for Aluminum=PmaxA=3755N12.19 mm2=308.04 MPa
Ultimate strength for Steel=PmaxA=7705 N12.44 mm2=619.373 MPa

  - % elongation for Aluminum=Lf-LiLi×100=108.87-100100×100=8.87%
% elongation for Steel=Lf-LiLi×100=106.08-100100×100=6.08%

  - Elastic modulus for Aluminum=σε=205.62 MPa0.003=69.54 GPa
lastic modulus for Steel=σε=498.91 MPa0.0029=172.038 GPa

  - % reduction of area for Aluminum=Af-AiAi×100=πrf2-AiAi×100=5.768-12.1912.19×100=52.68%
% reduction of area for Steel=Af-AiAi×100=πrf2-AiAi×100=4.6377-12.412.44×100=62.72%

  - Proportional limit for aluminum = 246,47 (MPa (from curve)
Proportional limit for steel = 402.46 MPa (from curve)

  - True fracture stress for Aluminum=P at fractureA=3224 N12.19 mm2=264.48 MPa
True fracture stress for Steel=P at fractureA=5325 N12.44 mm2=428.055 MPa

## Report

- Equipment includes the loading machine that can supply a tensile load to the metal sample used. Procedure is to secure the prepared sample onto the loading machine. Then using the pump slowly supply a tensile load to the sample and measure the deformation at each 500N. Do so until the sample fails. Finally measure the smallest diameter of the broken end.

## Discussion

- The stress-strain curve is more advantageous to the load-elongation curve because it gives more information as to the nature and characteristics of the material used. The stress is calculated with consideration with the area or the sample. With the load-elongation curve, it is very hard to get any information as to what the material is used. The stress-strain curve can give you the modulus of elasticity with is characteristic to each material.

- The elastic modulus of each material tells you about how much stress can a material take per deformation. A low modulus indicates that the material is more susceptible to deformation with the same amount of stress to a material with a high modulus. Steel has a higher modulus that aluminum, meaning that steel is more resistant to deformation when subjected to stress.

- Tensile properties might be different from the compressive properties of a material. How it takes stress in tension could be different to how it takes compression so results might be different.

- Ductility is the characteristic of a material to deform under tensile stress. A material with high ductility is one that can be stretched more before it fails compared to one with low ductility.

- Factors that could create discrepancies between the experimental and theoretical values include the states of the sample used, the equipment, etc. Since the measurements are rather small, even a slight % error in the data can create huge discrepancies. For instance there could be errors when measuring the diameter and length of the sample after failure.