March 25, 2015

ENGR 244

deflection of beams Lab #5

Teodor Matusoiu - 27509669

Objective

The goal of this experiment is to determine the theoretical deflection of different beams in order to determine the modulus of elasticity of three materials: Aluminum, Steel and Brass and then compare it to experimental values.

Introduction

When a beam is subjected to a transverse load, one can measure the deflection of the beam and by taking in consideration the magnitude, the location and the length span, various material properties can be found. It is common to assume that a higher deflection will take place in a longer beam. Deflection of a simply supported beam can be found through the derivation of the following formula :

Where:		=Radius of curvature

M= Bending moment

E= Modulus of elasticity

I= Moment of inertia

Materials and methods

All procedures were done according to ENGR 244 lab manual pages 18 to 24 and no modifications were made (Concordia Engineering Department 2015).

Results and Calculations

| Dimensions | Brass | Steel | Aluminum |
| --- | --- | --- | --- |
| Span Length, L (mm) | 455.00 | 455.00 | 455.00 |
| Width, w (mm) | 19.05 | 19.09 | 19.12 |
| Height, h (mm) | 12.77 | 12.79 | 12.81 |

| Cantilever Beam | Brass | Steel | Aluminum |
| --- | --- | --- | --- |
| Span, L (mm) | 250.00 | 250.00 | 250.00 |
| Height, h (mm) | 3.25 | 3.58 | 3.20 |
| Width, w (mm) | 19.16 | 19.02 | 19.11 |

| Cantilever Beam |  |  |
| --- | --- | --- |
| Brass |  |  |
| Load (g) | X=L deflection (mm) | X=0.5L deflection (mm) |
| 0 | 0 | 0 |
| 100 | -1.26 | -0.42 |
| 200 | -2.42 | -0.8 |
| 300 | -3.59 | -1.19 |
| 400 | -4.77 | -1.58 |
| 500 | -5.83 | -1.94 |

| Cantilever Beam |  |  |
| --- | --- | --- |
| Steel |  |  |
| Load (g) | X=L deflection (mm) | X=0.5L deflection (mm) |
| 0 | 0 | 0 |
| 100 | -0.61 | -0.19 |
| 200 | -1.16 | -0.37 |
| 300 | -1.68 | -0.54 |
| 400 | -2.24 | -0.74 |
| 500 | -2.74 | -0.92 |

| Cantilever Beam |  |  |
| --- | --- | --- |
| Aluminum |  |  |
| Load (g) | X=L deflection (mm) | X=0.5L deflection (mm) |
| 0 | 0 | 0 |
| 100 | -1.57 | -0.52 |
| 200 | -2.99 | -0.99 |
| 300 | -4.42 | -1.46 |
| 400 | -5.88 | -1.94 |
| 500 | -7.36 | -2.42 |

Simply-Supported Beams:

==

By integrating twice:

y=

With C1 = - and C2 = -

We get: Y=

For x = L/2 (Mid-Span)

Y= == -

For x = L/4 (Quarter-Span)

Y= == -

Sample Calculation

For steel:

I=112bh3

I=11219.09 mm*12.793 mm3

I≈3328.40mm4

I≈3.33*10-9 m4

| Theoretical Moment of Inertia (10^-9 m^4) |  |  |
| --- | --- | --- |
| Brass | Steel | Aluminum |
| 3.31 | 3.33 | 3.35 |

For mid span:

x=L2=0,4552=0.2275m

For quarter span:

x=L4=0,4554=0.11375m

Then the theoretical deflection for x at the mid span:

ytheo=

ytheo≈0.00089m≈0.89mm

| Theoretical Values |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Load (g) | Brass |  | Steel |  | Aluminum |  |
|  | at x = L/2 | at x = L/4 | at x = L/2 | at x = L/4 | at x = L/2 | at x = L/4 |
| 200 N | -1.13 | -0.78 | -0.59 | -0.41 | -1.67 | -1.15 |
| 400 N | -2.26 | -1.55 | -1.18 | -0.81 | -3.35 | -2.30 |
| 600 N | -3.39 | -2.33 | -1.77 | -1.22 | -5.02 | -3.45 |
| 800 N | -4.52 | -3.11 | -2.36 | -1.62 | -6.69 | -4.60 |
| 1000 N | -5.65 | -3.88 | -2.95 | -2.03 | -8.37 | -5.75 |

| Experimental Values |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Load (g) | Brass |  | Steel |  | Aluminum |  |
|  | at x = L/2 | at x = L/4 | at x = L/2 | at x = L/4 | at x = L/2 | at x = L/4 |
| 200 N | -1.35 | -0.96 | -0.65 | -0.5 | -1.74 | -1.26 |
| 400 N | -2.95 | -2.1 | -1.28 | -0.97 | -3.68 | -2.63 |
| 600 N | -4.57 | -3.26 | -1.95 | -1.47 | -5.6 | -3.99 |
| 800 N | -6.25 | -4.46 | -2.66 | -1.98 | -7.52 | -5.36 |
| 1000 N | -7.97 | -5.68 | -3.42 | -2.53 | -9.47 | -6.73 |

Using the Formulas:

For x = L/2 (Mid-Span)

Y =   E =

For x = L/4 (Quarter-Span)

Y =   E =

| Theoretical Modulus of Elasticity |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Load (g) | Brass |  | Steel |  | Aluminum |  |
|  | at x = L/2 | at x = L/4 | at x = L/2 | at x = L/4 | at x = L/2 | at x = L/4 |
| 200 N | 105.027 | 104.51 | 200.11 | 197.64 | 70.16 | 69.98 |
| 400 N | 104.981 | 105.19 | 199.94 | 200.08 | 69.95 | 70.01 |
| 600 N | 104.996 | 104.96 | 199.99 | 199.26 | 70.02 | 69.99 |
| 800 N | 105.004 | 104.85 | 200.02 | 200.08 | 70.05 | 69.98 |
| 1000 N | 105.008 | 105.05 | 199.97 | 199.58 | 69.99 | 70.00 |
| Average E | 105.003 | 104.91 | 200.01 | 199.33 | 70.03 | 69.99 |
|  | 104.958 |  | 199.67 |  | 70.01 |  |

| Error In Modulus Of elasticity |  |  |  |
| --- | --- | --- | --- |
| Beam Material | Brass | Steel | Aluminum |
| Published Value (GPa) | 105.00 | 200.00 | 70.00 |
| Experimental Value (Gpa) | 104.958 | 197.67 | 70.01 |
| Percentage Error (%) | 0.040 | 1.165 | 0.014 |

Part 2: Cantilever Beam

| Cantilever Beam |  |  |  |
| --- | --- | --- | --- |
| Cantilever Beam | Brass | Steel | Aluminum |
| Span, L (mm) | 250.00 | 250.00 | 250.00 |
| Height, h (mm) | 3.25 | 3.58 | 3.20 |
| Width, w (mm) | 19.16 | 19.02 | 19.11 |

Y=

For x = L

Y==  =

For x = L/2

Y==

Sample Calculations:

Applied force: 9.81 * (100/1000) = 0.98 N

Moment of Inertia for Brass: = 54.81 mm4 = 5.481 x 10-11 m4

At X = L => Using the above formula => Y=0.8869 mm

At X = L/2 => Using the above formula => Y=0.2771 mm

| Deflection of Cantilever Beam Brass |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Applied | Applied | Moment of | Experimental |  | Theoretical |  |
| Load (gm) | Load (N) | Inertia (mm4) | at x = L | at x = L/2 | at x = L | at x = L/2 |
| 100 | 0.98 | 54.811 | -1.26 | -0.42 | 0.887 | 0.277 |
| 200 | 1.96 | 54.811 | -2.42 | -0.8 | 1.774 | 0.554 |
| 300 | 2.94 | 54.811 | -3.59 | -1.19 | 2.661 | 0.831 |
| 400 | 3.92 | 54.811 | -4.77 | -1.58 | 3.548 | 1.109 |
| 500 | 4.91 | 54.811 | -5.83 | -1.94 | 4.444 | 1.389 |

| Deflection of Cantilever Beam Steel |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Applied | Applied | Moment of | Experimental |  | Theoretical |  |
| Load (gm) | Load (N) | Inertia (mm4) | at x = L | at x = L/2 | at x = L | at x = L/2 |
| 100 | 0.98 | 72.724 | -0.61 | -0.19 | 0.351 | 0.110 |
| 200 | 1.96 | 72.724 | -1.16 | -0.37 | 0.702 | 0.219 |
| 300 | 2.94 | 72.724 | -1.68 | -0.54 | 1.053 | 0.329 |
| 400 | 3.92 | 72.724 | -2.24 | -0.74 | 1.404 | 0.439 |
| 500 | 4.91 | 72.724 | -2.74 | -0.92 | 1.758 | 0.549 |

| Deflection of Cantilever Beam Aluminum |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Applied | Applied | Moment of | Experimental |  | Theoretical |  |
| Load (gm) | Load (N) | Inertia (mm4) | at x = L | at x = L/2 | at x = L | at x = L/2 |
| 100 | 0.98 | 72.724 | -1.57 | -0.52 | 1.381 | 0.431 |
| 200 | 1.96 | 72.724 | -2.99 | -0.99 | 2.761 | 0.863 |
| 300 | 2.94 | 72.724 | -4.42 | -1.46 | 4.142 | 1.294 |
| 400 | 3.92 | 72.724 | -5.88 | -1.94 | 5.523 | 1.726 |
| 500 | 4.91 | 72.724 | -7.36 | -2.42 | 6.918 | 2.162 |

| Applied | Applied | Moment of | Deflection exp. (mm) |  | Modulus of Elasticity (GPa) |  |
| --- | --- | --- | --- | --- | --- | --- |
| Load (gm) | Load (N) | Inertia (mm4) | at x = L | at x = L/2 | at x = L | at x = L/2 |
| 100 | 0.98 | 72.724 | -0.61 | -0.19 | 115.0581 | 200 |
| 200 | 1.96 | 72.724 | -1.16 | -0.37 | 121.0094 | 200 |
| 300 | 2.94 | 72.724 | -1.68 | -0.54 | 125.3312 | 200 |
| 400 | 3.92 | 72.724 | -2.24 | -0.74 | 125.3312 | 200 |
| 500 | 4.91 | 72.724 | -2.74 | -0.92 | 128.337 | 200 |
| Average experimental Modulus of elasticity (GPa) |  |  |  |  | 161.5 |  |
| % error from 200GPa Published Value (%) |  |  |  |  | 19.25 |  |

Discussion & Conclusion

- Compare the theoretical deflections with the experimental values.

- Determine the accuracy of the theoretical equations.

- Does the accuracy depend on the type of material, load machine, beam configuration? Discuss.

In comparing the theoretical deflection and the experimental values, it was found that the percent difference of the modulus of elasticity for brass, steel and aluminum are 0.04%, 1.16% and 0.014% respectively. These results are incredibly accurate, it could be said that suspiciously accurate. Nonetheless, this is proof that the measurements taken in the laboratory yielded accurate and precise data. Some discrepancies in the results could arise from errors in reading or measuring the dimensions, bad positioning of the beam, the precision of the measuring tools, the sample and its integrity and its fatigue.

- Comparing the modulus of elasticity, there is a much bigger difference in between the theoretical and experimental. The perfect differences for brass, steel and aluminum are 17%, 19% and 23% respectively. This could be due to the positioning of the weights on the cantilever setup as they were not stable and the difficulty in reading the measurement.

In conclusion, this laboratory can be deemed successful due to its rather low percent differences. As a lesson, one can learn that a bad design of a beam can have large consequences on its integrity and can cause failure in it.

References

Beer F. and Johnston, R. (1992) Mechanics of Materials, McGraw-Hill.