Civil Engineering Materials

CVG 2141

Lab I – Metals

Tensile Strength for Steel and Aluminum

Submitted by: Cyrus Hiranandani – 8471021

Lab date: September 23, 2016

Lab Group 13

Abstract

Tensile testing is a very fundamental aspect of Civil Engineering. Also referred to as a tension test, the subject is put under measured tension until the material fails. This is used to be able to predict how a subject would react when used and being put under different type of forces. The test allows us to come to standardized conclusions on specific materials, this includes; yield strength, tensile strength, and the breaking point. Having this information available allows the designer to compare the different materials side by side; giving them the opportunity to make the most educated decision on what material is the most ideal for their use.

Table of Contents

Graphs List ----------------------------------------------------------------------------------------------------1

Tables List -----------------------------------------------------------------------------------------------------1

Objective -------------------------------------------------------------------------------------------------------2

Background ----------------------------------------------------------------------------------------------------2

Equipment -----------------------------------------------------------------------------------------------------2

Procedure-------------------------------------------------------------------------------------------------------2

Data Presentation & Analytical Calculations -------------------------------------------------------------3

Discussion -----------------------------------------------------------------------------------------------------7

Conclusion-----------------------------------------------------------------------------------------------------8

References -----------------------------------------------------------------------------------------------------8

Graphs List

Graph 1 – Percent Elongation -------------------------------------------------------------------------------5

Graph 2 – Hot Rolled Steel ----------------------------------------------------------------------------------5

Graph 3 – Cold Rolled Steel --------------------------------------------------------------------------------6

Graph 4 – Aluminum -----------------------------------------------------------------------------------------6

Tables List

Table 1 – Cross Sectional Areas ----------------------------------------------------------------------------3

Table 2 - Hot Rolled Steel -----------------------------------------------------------------------------------3

Table 3- Cold Rolled Steel ----------------------------------------------------------------------------------3

Table 4 – Aluminum -----------------------------------------------------------------------------------------4

Table 5 – Area Reduction -----------------------------------------------------------------------------------4

Objective

Throughout the lab our objective was to determine the following:

- The stress-strain relationship

- The modulus of elasticity

- The elastic limit

- The tensile strength

- The rupture strength

- The resilience and toughness

- The percentage of elongation and the decrease in cross-sectional area

(Source: Lab Manual: “Lab 1 – Tensile Strength for Steel and Aluminum”, Page 1)

Background

Three different metal materials were put to a tensile test to determine the properties of each. From the data collected, we could use equations listed below to find our multiple properties of the sample using; Load, Cross Sectional area, Elongation, gauge length, stress and strain.

Materials are needed to withstand all sorts of different loads and forces at the same time. This experiment is one of the many that is used to make a complete and educated determination of which material is best used.

Strain equations:

σ = P/A (Load/Cross Sectional area)

ε=ΔL/L (Elongation/Gauge Length)

Modulus of elasticity:	   E = σyield/ εyield

Modulus of Toughness:  (σyield * εyield)/2 + ((σyield+ σrupture) (εrupture-εyield))/2

Equipment

Refer to: Lab Manual: “Lab 1 – Tensile Strength for Steel and Aluminum”, Page 1

Procedure

Refer to: Lab Manual: “Lab 1 – Tensile Strength for Steel and Aluminum”, Page 2

Data Presentation & Analytical Calculations

Sample calculation: W * H = A  19.13mm * 6.58mm = 125.8754mm2

Table 1 – Cross Sectional Areas

| Metal | Width(i) | Height(i) | Area(i) | Width(f) | Height(f) | Area(f) |
| --- | --- | --- | --- | --- | --- | --- |
| Cold rolled | 19.33667 | 6.48 | 125.3016 | 17.04 | 5.14 | 87.5856 |
| Hot rolled | 19.05333 | 6.33 | 120.6076 | 12.95 | 4.15 | 53.7425 |
| Aluminum | 18.88333 | 6.346667 | 119.8462 | 16.17 | 4.61 | 74.5437 |

Sample calculation:

((Lf - Li)/Li) * 100 = %E  ((35.10mm – 24.98mm) * 100) = 40.51%

Table 2 - Hot Rolled Steel

| Gauge # | Length(i) | Length(f) |  |  | Elongation (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 24.31 | 29.44 |  |  | 21.1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2 | 24.76 | 30.54 |  |  | 23.34 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3 | 25.77 | 39.19 |  |  | 52.08 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 | 24.54 | 30.92 |  |  | 25.99 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 | 24.99 | 30.52 |  |  | 22.13 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | 24.97 | 29.97 |  |  | 20.02 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7 | 25.56 | 29.90 |  |  | 16.98 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8 | 24.65 | 29.04 |  |  | 17.81 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9 | 25.23 | 28.97 |  |  | 14.82 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Table 3- Cold Rolled Steel |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Gauge # | Length(i) | Length(f) |  |  | Elongation (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | 24.91 | 28.98 |  |  | 16.34 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2 | 24.94 | 25.49 |  |  | 2.21 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3 | 24.94 | 25.28 |  |  | 1.36 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 | 24.94 | 25.35 |  |  | 1.64 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 | 24.76 | 25.06 |  |  | 1.21 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | 25.26 | 25.74 |  |  | 1.9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7 | 24.44 | 25.02 |  |  | 2.37 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8 | 25.09 | 25.63 |  |  | 2.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9 | 24.81 | 24.99 |  |  | 0.73 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Table 4 - Aluminum |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Gauge # | Length(i) | Length(f) |  |  |  | %Elongation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | 25.41 | 27.32 |  |  |  | 7.52 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2 | 24.86 | 27.79 |  |  |  | 11.786 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3 | 25.04 | 27.51 |  |  |  | 9.86 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 | 25.28 | 31.79 |  |  |  | 25.75 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 | 25.11 | 28.29 |  |  |  | 12.66 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | 25.10 | 27.68 |  |  |  | 10.28 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7 | 25.28 | 27.48 |  |  |  | 8.7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8 | 24.97 | 27.22 |  |  |  | 9.01 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9 | 24.73 | 27.15 |  |  |  | 9.79 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Sample calculation:

%Area Reduction = -((Af-Ai)/Ai)*100%

-(57.39-121.66)/121.66*100% = 52.83%

Table 5 – Area Reduction

| Specimen | Ai | Af | Area Reduction % |
| --- | --- | --- | --- |
| Cold-rolled Steels | 125.3016 | 74.5437 | 40.51 |
| Hot-rolled Steels | 120.6076 | 53.7425 | 55.44 |
| Aluminium | 119.8462 | 74.5437 | 37.8 |

Graph 1 – Percent Elongation

Graph 2 – Hot Rolled Steel

Graph 3 – Cold Rolled Steel

Graph 4 - Aluminum

Rupture Strength

Hot-rolled Steel = 528.9534N/mm^2

Cold-rolled Steel = 841.9765N/mm^2

Aluminum = 303.771N/mm^2

Hot-rolled steel

Max load = 47949N

Max elongation = 10.4503mm

σ = P/A = 47949 N/120.6076mm^2 = 397.562N/mm^2

ε=ΔL/L = 10.4503mm/50mm = 0.209006

Cold-rolled Steel

Max load = 85004.3N

Max elongation = 0.434925mm

σ = 85004.3N /125.3016mm^2 = 678.3976N/mm^2

ε = 0.434925mm /50mm= 0.008699

Aluminum

Max load = 28570.5N

Max elongation = 8.05635mm

σ = 28570.5N /119.8462mm^2 = 238.393N/mm^2

ε = 8.05635mm/50mm = 0.161127

Modulus of elasticity = σyield/ εyield

Hot-rolled Steel = (397.562N/mm^2)/ 0.209006 = 1902.156N/mm^2

Cold-rolled Steel = 77.986 kN/mm2

Aluminum = 1479.535N/mm2

Modulus of Resilience = (σyield* εyield)/2

Hot-rolled Steel = (397.562N/mm^2)*( 0.209006)/2 = 41.55N/mm^2

Cold-rolled Steel = 2.99 N/mm^2

Aluminum = 19.2 N/mm^2

Discussion

We focused on three different metal types that are used in the real world today. These are hot rolled steel, cold rolled steel, and Aluminum.

Hot-rolled steel is tough, it has the ability to retain large amount of loads or tensile forces. The deformation was the most obvious of all the metals. It is not very brittle, but withholds loads and experiences hardening which makes it extra tough. The largest deformation occurred at point 3.

Cold-rolled steel retains the largest force without deformation. It becomes brittle, thus it does not hold large loads to undergo hardening. It does break very shortly after the yield point and really is not that tough. The largest deformation occurs at point 1.

Aluminum is a soft metal in comparison to the other two. It does not have an obvious yielding point; as seen in the graph. The stress is much lower than both steels. All calculations also tend to be lower than steels. It deformed the least which means the area reduction and elongation are both lower than steel.

Source of Error

Measuring the cross sectional area may not have been as precise as it could be due to the width of the calliper did not completely fit into the grooves of the break. As well, the measuring itself may have been inconsistent, i.e. starting at the middle of the groove to the end of the groove rather than middle to middle.

Conclusion

The lab was successful, we found the stress-strain relationship, proportional limit, yield stress,  Young’s modulus of elasticity, modulus of toughness, modulus of resilience, rupture strength, tensile strength, percent elongation and reduction in cross-sectional area of each specimen. This information gives us better insight on the pros and cons of each to make an educated decision on which to use in what situation.

Hot rolled steel is easy to deform but can withhold great load. Cold-rolled steel is brittle but can take the largest load before rupture. Aluminum deforms the least but withstand least of force as well.

References

Lab Manual: “Lab 1 – Tensile Strength for Steel and Aluminum”