Experiment No.2: Tension Test on Metals

Lab Section: LI-X

Wednesday February 19th, 2020

Objective:

The main purpose of this lab was to apply a tension test on steel and aluminum and observing the deformation, stress and strain that occurs.

Introduction:

The tension test is utilized to determine the maximum stress a material can sustain by applying an axial force. We gradually apply the force slowly extending the specimen until it fractures. During this process, we record the elongation of the gauge and the force applied. This data is used to measure the engineering strain, ɛ, and the engineering stress, σ. Once we obtain that information, we can graph a stress-strain curve. This graph allows us to determine many other properties such as the material ultimate strength, yield strength and the modulus of elasticity. Also, we can predict how a material will perform under different type of forces which helps in choosing the material needed for specific projects. We can assume that steel will have a higher ultimate strength comparing to aluminum.

Equipment:

- Tension testing machine

- Deformation measurement device

- Vernier Caliper

- Steel and aluminum specimens

- V-groove tray

Procedure:

- Measure the diameter of the specimens, aluminum and steel, using the Vernier calipers. Assume the specimens have a gauge length of 100 mm.

- Set the specimen in the deformation measurement device. Ensure that the two set of screws are secures as seen in the figure below and zero the reading.

Figure11

- Ensure that the load read-out is zero as well.

- Install the screw-on caps at the end of the gauge. After tightening it all the ways, unscrew it by half a turn and mount it on the testing machine.

- For steel: Apply force slowly and steadily and document the deformation every 500N until 5000N is reached. After 5000N document the deformation every 200N. Once the load stops increasing or decreases, document the data based on deformation increment: every 0.25mm.

For Aluminum: Apply force slowly and steadily and document the deformation every 500N until 5000N is reached. After 5000N document the deformation every 200N. Once the load stops increasing or decreases, document the data based on deformation increment: every 0.50mm.

- Once failures occur, document the maximum load and measure the final length using the v groove and the deformation machine while keeping the two screws as shown in the figure below.

Figure 21

- Measure the smallest final diameter of the specimen where the fractures occurred.

Results:

|  | Before Fracture |  | After Fracture |  |
| --- | --- | --- | --- | --- |
|  | Initial Length (mm) | Initial Diameter (mm) | Final Length (mm) | Final Diameter (mm) |
| Steel | 100 | 4.02 | 103.31 | 2.84 |
| Aluminum | 100 | 4.99 | 111.34 | 2.65 |

Table 1.1

| Steel |  |  |  |  |
| --- | --- | --- | --- | --- |
| Load P (N) | Deformation(mm) | d(mm) | Strain | Stress (Mpa) |
| 519 | 0 | 100 | 0 | 40.89 |
| 1001 | 0 | 100 | 0 | 78.87 |
| 1506 | 0.02 | 100 | 0.0002 | 118.65 |
| 2020 | 0.04 | 100 | 0.0004 | 159.15 |
| 2505 | 0.08 | 100 | 0.0008 | 197.36 |
| 3012 | 0.08 | 100 | 0.0008 | 237.31 |
| 3500 | 0.12 | 100 | 0.0012 | 275.76 |
| 4004 | 0.15 | 100 | 0.0015 | 315.47 |
| 4503 | 0.18 | 100 | 0.0018 | 354.78 |
| 5014 | 0.2 | 100 | 0.002 | 395.04 |
| 5191 | 0.22 | 100 | 0.0022 | 408.99 |
| 5405 | 0.22 | 100 | 0.0022 | 425.85 |
| 5597 | 0.24 | 100 | 0.0024 | 440.97 |
| 5799 | 0.24 | 100 | 0.0024 | 456.89 |
| 5994 | 0.26 | 100 | 0.0026 | 472.25 |
| 6205 | 0.27 | 100 | 0.0027 | 488.88 |
| 6402 | 0.27 | 100 | 0.0027 | 504.40 |
| 6798 | 0.34 | 100 | 0.0034 | 535.60 |
| 6998 | 0.42 | 100 | 0.0042 | 551.36 |
| 7202 | 0.45 | 100 | 0.0045 | 567.43 |
| 7405 | 0.7 | 100 | 0.007 | 583.42 |
| 7472 | 1.01 | 100 | 0.0101 | 588.70 |
| 7448 | 1.27 | 100 | 0.0127 | 586.81 |
| 7468 | 1.51 | 100 | 0.0151 | 588.39 |
| 7428 | 1.76 | 100 | 0.0176 | 585.23 |
| 7444 | 2.01 | 100 | 0.0201 | 586.50 |
| 7166 | 2.26 | 100 | 0.0226 | 564.59 |
| 6980 | 2.53 | 100 | 0.0253 | 549.94 |
| 6841 | 2.78 | 100 | 0.0278 | 538.99 |
| 6511 | 3.08 | 100 | 0.0308 | 512.99 |
| 6164 | 3.28 | 100 | 0.0328 | 485.65 |
| 5655 | 3.52 | 100 | 0.0352 | 445.54 |

Table 1.2

| Aluminium |  |  |  |  |
| --- | --- | --- | --- | --- |
| Load P (N) | Deformation(mm) | d(mm) | Strain | Stress (Mpa) |
| 529 | 0.04 | 100 | 0.0004 | 27.05 |
| 999 | 0.04 | 100 | 0.0004 | 51.08 |
| 1442 | 0.04 | 100 | 0.0004 | 73.74 |
| 1976 | 0.06 | 100 | 0.0006 | 101.04 |
| 2464 | 0.09 | 100 | 0.0009 | 125.99 |
| 2961 | 0.19 | 100 | 0.0019 | 151.41 |
| 3502 | 0.23 | 100 | 0.0023 | 179.07 |
| 4012 | 0.27 | 100 | 0.0027 | 205.15 |
| 4501 | 0.27 | 100 | 0.0027 | 230.15 |
| 5017 | 0.36 | 100 | 0.0036 | 256.54 |
| 5230 | 0.37 | 100 | 0.0037 | 267.43 |
| 5402 | 0.5 | 100 | 0.005 | 276.23 |
| 5514 | 1 | 100 | 0.01 | 281.95 |
| 5549 | 1.52 | 100 | 0.0152 | 283.74 |
| 5531 | 2.01 | 100 | 0.0201 | 282.82 |
| 5619 | 2.5 | 100 | 0.025 | 287.32 |
| 5649 | 2.96 | 100 | 0.0296 | 288.86 |
| 5677 | 3.5 | 100 | 0.035 | 290.29 |
| 5574 | 3.94 | 100 | 0.0394 | 285.02 |
| 5731 | 4.49 | 100 | 0.0449 | 293.05 |
| 5817 | 5.01 | 100 | 0.0501 | 297.45 |
| 5870 | 5.47 | 100 | 0.0547 | 300.16 |
| 5897 | 5.98 | 100 | 0.0598 | 301.54 |
| 5910 | 6.51 | 100 | 0.0651 | 302.20 |
| 5928 | 7.03 | 100 | 0.0703 | 303.12 |
| 5886 | 7.51 | 100 | 0.0751 | 300.97 |
| 5820 | 7.99 | 100 | 0.0799 | 297.60 |
| 5931 | 8.49 | 100 | 0.0849 | 303.28 |
| 5901 | 9.01 | 100 | 0.0901 | 301.74 |
| 5786 | 9.52 | 100 | 0.0952 | 295.86 |
| 5412 | 10 | 100 | 0.1 | 276.74 |
| 4792 | 10.49 | 100 | 0.1049 | 245.03 |
| 3844 | 11.03 | 100 | 0.1103 | 196.56 |
| 3398 | 11.34 | 100 | 0.1134 | 173.75 |

Table 1.3

The stress was obtained using the following formula:

σ=PA

Where:

σ = Tensile stress on the specimen (MPa)

P = Load applied on the specimen (N)

A = Cross section area of the specimen (mm2)

Sample Calculation:

Steel 6th entry

A=π(2.01)2=12.692 mm2

σ= 3012 (N)12.692 (mm2)=237.31 (MPa)

The strain was obtained using the following formula:

ε=δL

Where:

ε = Strain (mm/mm)

L= Gauge length (mm)

δ = Elongation (mm)

Sample Calculation:

Steel 6th entry

ε= 0.08 (mm)100 (mm)=0.008

Engineering Stress-Strain Curve:

Graph 1.1

Graph 1.2

Fractured Specimens: We did not take clear pictures of the fractured specimens. We have two screenshots from the video we recorded. We also included a picture to demonstrate what the fracture looked like.

- Steel:

Our video screenshot		A look-like of the fracture5

- Aluminum:

Our video screenshot			A look-like of the fracture6

The following properties were determined from the data collected:

|  | Steel | Aluminum |
| --- | --- | --- |
| Yield Strength (MPa) | 395.04 | 151.41 |
| Ultimate Strength (MPa) | 589.10 | 306.04 |
| Percent of Elongation % | 3.31% | 11.34% |
| Elastic Modulus (GPa) | 132.405 | 50.513 |
| Percent Reduction of Area % | 50.09% | 72.01% |
| Proportional Limit (MPa) | 504.40 | 267.43 |
| True factor stress (MPa) | 892.70 | 616.09 |

Table 1.4

Sample Calculation:

Steel Specimen

Yield Strength

Yield Strength is the stress were plastic deformation occurs.  At ε=0.002 we traced a line to the slop of the curve which fives us the yield strength of material.

For steel it 395.04 MPa.

Ultimate Strength

We can obtain the ultimate stress, by calculating the stress with the maximum load.

σ=PmaxA=7477 N12.69 mm2=589.10 MPa

Percentage of Elongation:

EL=Lf-LiLi x 100

Where

Lf = Final Length

Li = Initial Length

EL=(103.31-100) mm100 mm  x 100=3.31%

Elastic Modulus:

The Elastic Modulus is the slop of the linear curve:

E=∆σ∆ε

where

Δσ = the variation of stress

Δε = the variation of strain

E=488.8772-237.3083 MPa(0.0027-0.0008) × 0.001 GPa1 Mpa=132.405 GPa

Percent Reduction of Area:

RA=Ai-AfAi ×100

Where

Ai = Initial Area

Af = Final Area

RA=12.69-6.3312.69 ×100= 50.09%

Proportional Limit:

The proportional limit is the point in the stress-strain curve where we go from linear to nonlinear, in other words from elastic deformation region to plastic deformation. In our case for steel, it is at 504.40 Mpa.

True factor stress

σ=PfAf=5655 N6.33 mm2=892.70 MPa

Where

Pf = Load at fracture

Af = Area at fracture

Discussion and Conclusion:

- A load-elongation curve is dependant on the material cross sectional area whereas an engineering stress-strain diagram is independent on area of cross section. For example, we just performed a test with an aluminium sample with a specific cross-sectional area, if we graph the load-elongation diagram, we would have to repeat the same test for any other aluminum with a different cross section area. However, this is not the case with the stress-strain diagram, it allows us to do the test once and extract all information necessary such as yield strength, ultimate strength and Modulus of elasticity for any shape aluminum sample.

- With the modulus of elasticity, E, we can determine how much the material will elastically stretch when force is applied. The higher the value of E the stiffer the material. For our samples, we can determine that steel has a higher stiffness than Aluminum with 132.405 MPa and 50.513 MPa, respectively.

- If we were to test the same specimens in compression instead of tension, we would have slightly different material properties. In compression we are applying the force towards the specimen comparing to tension we are pulling the specimens which causes different failure. Tension stress causes the specimens to fail much faster than compression.

- Ductility is the ability of a material to go under permanent deformation before fracturing.  The bigger the amount of plastic deformation before it breaks the more ductile the material. The parameters that are indicators of ductility are the percent of elongation and the percent of reduction of area.

- Table is comparing our tested results with the one provided in the lab Manuel.  We can see that the tested value of the ultimate strength is very close to the expected values for both specimens. Whereas the percentage of elongation for the aluminum is closer to it’s true value comparing to the steel value.

- Stress strain diagram is  independent  of the material cross sectional

- area. As area is always changing during a tensile test, true stress is

- difficult to measure. True stress is when we divide the applied force by

- the instantaneous cross sectional area of the specimen.

- That’s why  we  normalize force  with  its cross  section.  We call  it  an

- Engineering  stress  and  it is   more common. True  stress  is  used for

- deformation   processes.  A   load-elongation   curve   applies   only   to   the

- geometry of the tested material. A stress-strain diagram applies to the

- material itself, in any geometry. So if for example we test an aluminum

- sample and get the stress-strain curve, we can apply this diagram to

- every   aluminum   sample     no   matter   it’s   geometry   nut   with   load-

- elongation diagram we have to repeat every time the test because the

- geometry of the sample is not the same. From stress-strain curve it’s

- easier to get the information such as yield strength, tensile strength,

- modulus

| Property | Aluminium (6061-T6) | Aluminium Tested | Steel (C12 L14) | Steel Tested |
| --- | --- | --- | --- | --- |
| Yield Strength (MPa) | 275 | 151.41 | 415 | 395.04 |
| Ultimate Strength (MPa) | 310 | 306.04 | 540 | 589.1 |
| % Elongation | 12 | 11.34 | 10 | 3.31 |
| Mod. of Elasticity (GPa) | 69 | 50.52 | 200 | 132.24 |

Table 1.5

The discrepancy occurs from the following possible source of errors:

  - We experienced some difficulties with our deformation measurement device. When we initially started our experiment with the steel sample, the deformation measurement device was not recording any data. This resulted in us having to restart the experiment with a different specimen.

  - While mounting the specimens on to the testing machine, we tried to keep it as aligned as possible with the y-axis. However, there must have been some axial misalignment which caused the break to not occur at mid point.

  - We recorded the process in order to be able to collect the data as closely as possible, nevertheless the force applied was manual and the data collected was with the naked eye. This could’ve caused some human error in our data analysis.

In conclusion, our assumption made during the introduction were right, the ultimate strength for steel was higher than aluminum. Steel has an ultimate strength of 589.1 MPa whereas aluminum is 306.04 MPa.

References:

- Mechanics of Material, Lab Manuel, experiment 2 p.6

- https://en.wikipedia.org/wiki/Tensile_testing

- https://sciencing.com/calculate-ductility-5417121.html

- https://physics.info/elasticity/summary.shtml

- https://www.mtu.edu/materials/k12/experiments/tensile/

- https://pdfs.semanticscholar.org/884e/2d0d104bcb07da95d54045a0016aad4b4356.pdf

- https://www.instron.com.br/pt-br/our-company/library/glossary/p/proportional-limit